## Slide 1
Lecture 10
Chemical Engineering for Micro/Nano Fabrication
Minoan Signet Ring
From the Bronze Age

## Slide 2: Birefringent Crystals
CaF2
CaCO3

## Slide 3: Frogs

## Slide 4
Pattern Density Effects
Easiest… Easy… Very Difficult!
“Residual layer”

## Slide 5: Step and Flash Imprint Lithography
S-FIL fluid dispenser
Ink jet system
Planarization layer
Substrate
Step 1: Dispense drops
Step 2: Lower template and fill pattern
Step 3: Polymerize S-FIL fluid with UV exposure
Step 4: Separate template from substrate
Template
Substrate
Substrate
Template
Step & Repeat
Substrate
Planarization layer
Planarization layer
Planarization layer
Fused silica template, coated with release layer
Template filling driven by capillary action
low imprint pressure and room temperature process
Template
Notes: So how does the technology work. Well before I go into the details of SFIL, lets talk about imprint technology in general. It had its genesis I suppose with the wax seals that the Chinese invested to authenticate documents, and the same thermoplastic process has been used in the past decade to make very high resolution lithography patterns – with Stephen Chou at Princeton leading the way. However, any thermal process is an absolute non starter in the CMOS industry since it makes accurate overlay impossible. The next alternative was to use a UV curable film spun onto the wafer, but now you have the challenge of moving a relative high viscosity material between the various patterns on the template, so Grant and SV came up with the idea of using a low viscosity monomer placed on the surface of the wafer.
This slides shows a schematic animation of the SFIL process:
Points to make – template is common with photolithography – smaller dimensions yes, but otherwise common to allow commercial supply – no membranes per previous NGL efforts
- process leaves a very thin film which can be removed in an etch descum. ie the process is compatible with etch. Thus the upstream template and the down stream etch and compatible. Just replace the litho cell.
- some application are whole wafer

## Slide 6
S-FIL vs. Optical Lithography Schematic
Greatly simplified and lower cost process
Standard Optical Lithography
Imprint Lithography

## Slide 7: First Publication of SFIL
Matt Colburn, et. al
Colburn, et.al “Step and Flash Imprint Lithography: A New Approach to High-Resolution Patterning,” Proc. SPIE 3676 379-389 (1999)
First SFIL tool
40 nm images

## Slide 8
“Issues” with SFIL are:
S.V. Sreenivasan
Residual Layer
Templates
  Orientation control
  Making 1X templates
Residual layer control
Defects
  Template wear
Alignment
Throughput
Templates
  Orientation control
  Making 1X templates
Residual layer control
Defects
  Template wear
Alignment
Throughput

## Slide 9: Self-Leveling Scheme using Template Flexure
Z head
Wafer
Wafer Tip/Tilt stage
Theta stage
XY stage
Template
flexure
Template
chuck
Template
calibration stage
Template
Remote center
of rotation
Template
Template-substrate interface
Flexure Schematic
B. J. Choi, S. Johnson, M. Colburn, S.V. Sreenivasan, C. G. Willson, “Design of Orientation Stages for Step and Flash Imprint Lithography,” Journal of Int. Societies for Precision Engineering and Nanotechnology, Volume 25, No. 3, pp. 192-199, July, 2001.

## Slide 10: Modern Imprint Head…MII and Canon

## Slide 11: SFIL tool decade later

## Slide 12: SFIL Lithography
2nm Replication
(Rogers et al, Illinois)
26 nm metal 1
Line and 100 nm via
11nm lines and spaces
14 nm posts
Notes: This process provides remarkable resolution. Essentially, what ever can be put into the template can be replicated in this process. It is possivle to copy 2 nm images as shown, images that have more than one level and lines and dots simultaneously.

## Slide 13: Gate Level: 38nm Half Pitch

## Slide 15: Claims of competitors and detractors
Obviously, you cannot …….
control residual layer thickness
manage defects….no pellicle???
achieve layer to layer alignment
achieve workable throughput
Abut fields, etc, etc.

## Slide 16: Residual Layer Thickness Control
Residual layer needs to be thin and uniform
Residual Layer is due to the inevitable undisplaced liquid
Residual Layers
Residual Layer
Avoid: Non-uniformities

## Slide 17: Focus on Continuous Process Improvement
  Minimize mean and standard deviation of residual layer
  Key drivers: chuck flatness, inkjet drop volume and location controls, evaporation.
1.
3.
4.
2.

## Slide 18: Residual Layer Thickness Measurements Early Results
Residual layer mean <20nm and thickness variation to < 6 nm TIR
Residual layer thickness fully populated wafer
28 nm HP

## Slide 19: Residual Layer Control Today
Software and hardware have been developed to correctly jet resist, and control the spreading of the resist.

## Slide 20: 1) Why do you think 1X projection lithography replaced contact printing in the early 80’s?? Don’t you learn from history?? 2) Do you propose attempt to do lithography without a pellicle??!!
Defects

## Slide 21: Template Before and After Imprints
All visible defects disappear from
the template.
Printing is the best way to clean
an SFIL template!
This is our “Pellicle”
Template prior to imprint
Template after second imprint
Filthy
Template

## Slide 22: Defect Density Trend Similar to Immersion….early work
Data measured on imprinted wafers – includes all sources of defects
Steady improvement in defect density –
Rate approximately one order of magnitude per year
  very similar to immersion lithography learning curve

## Slide 23: Defect Control in the current Canon Tool
1 particle / 2500 wafers !

## Slide 24: Electrical Testing for Defectivity
Serpentine conductor testing

## Slide 25: Field-To-Field Alignment
Moiré metrology originally developed for X-Ray litho (Smith, Moon)
  Sub-nanometer resolution, inclined optics
  Insensitive to film thickness variations
Alignment and scale/shape correction are performed “in-liquid” which is typically a 15nm residual layer
25

## Slide 28: Overlay: Scale/Shape Correction Mechanism
SiC Chuck & Template
Loadcell
Gimbal
Pads
28

## Slide 29: High Order Corrections

## Slide 30: 3 sigma alignment SFIL to 193 nm Optical

## Slide 32: Throughput
Full Wafer printing is not possible now
  Here alignment is the issue
Fill time is the rate limiting step
  Control of dispense pattern
  Resist material design
Engineering the separation step
  Minimize defects
  Maximize template life time

## Slide 33: The Fill Step Adaptive dispense, spread and release in 1.5 sec

## Slide 34: The Fill Step

## Slide 35: The Fill Step

## Slide 36: The Fill Step

## Slide 37: The Fill Step

## Slide 38: Snap Shots of previous steps

## Slide 39: Nanofluidics: RLT Control and High Throughput
High density
Med Density
Low Density
Drop dispense addresses template geometry variation, pattern-specific directionality of flow, multi-scale fluid/solid mechanics, etc. Need to solve inverse problem.
√
39