## Slide 1
Lecture 11
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Surface Energy and Surface Tension
https://knowledge.ulprospector.com/3354/pc-surface-tension-surface-energy/
Surface Energy
High Medium Low

## Slide 3: Contact angle and surface energy
goniometer

## Slide 4: The silicon resist design for high aspect ratio
Organosilicon imprint with residual layer
Planarizing overcoat
(Ultra-High Si-mat)
organosilicon imprint after residual layer etch
High aspect ratio pattern
after selective etch
Selective O2 RIE does not
Etch organosilicon material
SUBSTRATE
SUBSTRATE
SUBSTRATE

## Slide 5: Early imprint results

## Slide 6: Imprint Resist Formulation a System Problem
Release layer
Adhesion layer:
(covalent bonding with
resist during UV cure)
substrate
template
Resist: Photopolymerizable monomers initiator and reactive surfactant

## Slide 7
Cohesive vs Adhesive Separation
Material with poor mechanical properties
Cohesive Failures call for stronger materials
Fouled Templates due to
Bad Materials Properties

## Slide 8: First Etch Barrier Formulation
Well defined,
stable structures:
Low viscosity: 1.9cPs/20C
Rapid cure to high conversion:
Si-containing monomer
EGDA
t-BuAc
Darocur 1173
40nm
30nm

## Slide 9: Role of Evaporation in Imprint Process
Thin residual layers and ease of filling require low viscosity & small drops.
High evaporation can lead to:
  Variable mechanical properties of imprint material
  Variation in film thickness
Evaporation of an 80pL Drop of Monomer |  |  |  |  | 
Initial Drop | 10 seconds | 20 seconds | 30 seconds | 40 seconds | 50 seconds
70m
~ 42% material loss
~ 56% material loss
Notes: -Turn your attention from the dispenser to the drops the it is jetting …
-Low viscosity fluids are inherently volatile and will evaporate, which can create variable mechanical properties of the imprint material and give rise to variation in the residual layer thickness.
-To study evaporation, we use the age sessile drop method shown here…
-After 30sec of evaporation, 42% of the material is loss … how it can influence the mechanical robustness of the imprint
-I will show you an example of how we have addressed this situation …

## Slide 10
Re-working etch barrier formulation
SIA0210 44%
EGDA 15%
iBA 37%
Irgacure 4%

## Slide 11
Old Stuff
New Stuff
Elongation at break 1-2%
Elongation at break 30-35%
Tensile Modulus 80 MPa
Tensile Modulus 500 MPa

## Slide 12
Many fold improvement in mechanical properties
by controlling partial pressure of constituents
0
5
10
15
20
25
30
35
5.0x10
6
1.0x10
7
1.5x10
7
Old Stuff
Stress (Pa)
Elongation (%)

## Slide 13
Template Release issues
Fluorinated Self Assembly Monolayer (F-SAM)
Solution?
Silicon dioxide (quartz) has high surface energy
Fluorocarbons like teflon have very low surface energy

## Slide 14
Template Release issues

## Slide 15: Adhesion Test Tool

## Slide 16: Imprint on an Instron

## Slide 17: Instron Experiment

## Slide 18: Fluorosurfactant additives
2-(Perfluorodecyl)ethyl acrylate (R)
Methyl perfluorooctanoate (NR)

## Slide 19: XPS or ESCA analysis
XPS X-ray photoelectron spectroscopy
ESCA (electron spectroscopy for chemical analysis)

## Slide 21: Contact angle and surface energy
goniometer

## Slide 22
Bad News!
81 imprints maximum
Water contact angle (degree)
The numbers of imprints
0
20
40
60
80
100
120
0
10
20
30
40
50
60
70
80
90
100

## Slide 23
We have a “wear” problem
Fluorinated Self Assembly Monolayer (F-SAM)
Current solution & a problem
Imprints
Degradation & defects !!

## Slide 24
Solution to the “wear” problem
HMDS
Fluorinated silazane
Comparable structure to F-SAM !!!
Replenish !!!
Imprints
w/ F-silazane
Imprints
F-SAM
Degraded …
Concept
A reactive surfactant

## Slide 25
Multiple Imprints Results
81 shots
hard more imprints
100 shots
possible more imprints
Water contact angle (degree)
The numbers of imprints

## Slide 26
10,000 non-stop Imprints for one Template
Defect Template
Wafer layout
Imprinted 82 - 200mm wafers with 124 fields per wafer
Wafers were imprinted with 13 mm X 13 mm mask fields
The imprints had no unprinted streets between the imprints
No process disruptions due to particles were observed
Do not know of any limitations, we could have printed more fields