## Slide 1
Lecture 13
Chemical Engineering for Micro/Nano Fabrication
Damascene

## Slide 2: Reverse Tone Etch Process: “S-FIL/R” (Lower aspect ratio features, thick residual layer, topography)
thick residual layer of organic material
Planarizing overcoat
(High Si content)
Organic material
Si material after blanket etch back or CMP
High aspect ratio pattern
after selective etch
Selective and anisotropic O2 RIE
SUBSTRATE
SUBSTRATE
SUBSTRATE
Low aspect ratio imprint
Advantages of SFIL-R
faster fill
tone reversal

## Slide 3: Canon, Toshiba and SK hynix going forward with SFIL
Revolutionizing the Semiconductor Industry - Nanoimprint Lithography
Report: Toshiba adopts imprint litho for NAND production
June 07, 2016 // By Peter Clarke
Toshiba will adopt nanoimprint lithography (NIL) as a way of reducing the cost of production of NAND flash memory, according to a Nikkei report. Toshiba plans to allocate part of an 860 billion yen (about $8 billion) budget for spending on semiconductors over the next three years on introducing NIL into flash memory production lines, the report said. Production is set to begin in fiscal 2017 in Yokkaichi.

## Slide 4: News Release
Canon provides nanoimprint lithography manufacturing equipment to Toshiba Memory's Yokkaichi Operations plant
TOKYO, July 20, 2017—Canon Inc. announced today that the company has provided the FPA-1200NZ2C, semiconductor lithography equipment that utilizes nanoimprint lithography (NIL) technology which Canon has been continuously developing since 2004, to leading provider of semiconductor memory solutions Toshiba Memory Corporation's Yokkaichi Operations plant. The provision of this equipment represents significant progress toward semiconductor device mass production that employs nanoimprint technology.

## Slide 5
https://semiengineering.com/what-happened-to-nanoimprint-litho/
What Happened To Nanoimprint Litho?
Next-gen lithography technology resurfaces for a variety of tasks.
MARCH 29TH, 2018 - BY: MARK LAPEDUS
Nanoimprint lithography (NIL) is re-emerging amid an explosion of new applications in the market……….. Toshiba installed Canon’s latest NIL system in a fab in Japan. If all goes well, Toshiba plans to use Canon’s system to pattern some of the features for its 3D NAND devices, as well as next-generation memory types in the future. Production is slated for later this year. “We hope nanoimprint will be ready for production soon,” said Tatsuhiko Higashiki, senior fellow

## Slide 6: Non-CMOS Applications
Photonic Crystals
Patterned
Media
100nm
20 nm
100 nm

## Slide 7
Damascus Syria

## Slide 8: The Damascene Process
https://www.damascenejewelry.net/content/4-about-damascene-jewelry

## Slide 9: The Damascene Process

## Slide 10: The Damascene Process

## Slide 11: The Damascene Process

## Slide 12: The Damascene Process

## Slide 13: Damascene Process

## Slide 14: Damascene Swords and Jewelry

## Slide 15: Damascene Swords and Jewelry
https://www.youtube.com/watch?v=mgP2ENTwwTE

## Slide 16: Damascene Swords and Jewelry

## Slide 17: Interconnect levels “back end of the line”…BEOL

## Slide 18
Moore
You?
These structures are made by “damascene”. Can we make them more efficiently and at lower cost by SFIL???

## Slide 19
Traditional
Dual Damascene Process
Dual Damascene Process
with Imprint Litho
Dual Damascene Process
resist
etch stop
substrate
ILD
ILD
Initial stack
Trench litho
Trench etch
Resist ash
BARC / resist
Via litho
Via etch
Resist Ash
Barrier
Cu metal
CMP
Initial stack
Imprint
Breakthru etch
Cure
dielectric precursor
etch stop
substrate
Barrier
Cu metal
CMP
184 steps for 8 levels of Cu
72 steps for 8 levels
ILD = inter layer dielectric

## Slide 20
Dispense SIM Material
SFIL Damascene Process (SIM)
# of process steps:
Multi-Tier Template
Position template
Flash
Release
SFIL IMPRINTING
M1
1
Deposit barrier
Deposit CVD dielectric (BD)
CVD Dielectric
2
3

## Slide 21
SFIL Damascene Process
# of process steps:
0
Sacrificial Imprint Material (SIM)
4
M1
CVD Dielectric
Etch Transfer
5
Strip (SIM)

## Slide 22: SFIL Damascene Process
M1
Etch Diffusion Barrier
Copper Seed
Copper Plate
# of process steps:
6
7
8
9
184 – 72 = 112 Saved steps ?
x 8
72
CMP

## Slide 23: BEOL Multilevel Imprint Cost Saving
20% overall saving at 30 wph
Cost analysis courtesy of Sergei V. Postnikov, Infineon Technologies
20%

## Slide 24: Chemical Mechanical Polishing

## Slide 25: CMP Tools

## Slide 27: Via Chain Test Structure
M2
V2
M1
2.5um
1.5um

## Slide 28: Via Chain Structures
100nm vias
100nm via
100nm vias
M2 by SFIL
M1 by
Photolithography
Via chain

## Slide 29
Via chain test site
Template
now a commercial product

## Slide 30: Imprinting

## Slide 31: Pattern Transfer Demonstration
Trench
Etch
CF4/C4F8/N 2
Ash
N2/H2
Both Coral® and Black Diamond® were processed

## Slide 32: Wiring Level Complete
After etch
After metal
After metal
If this works, it saves more than 100 unit process steps from the manufacturing of a modern microprocessor and provides a saving of 20-50% (per studies by Infineon and SEMATECH)

## Slide 33: Wiring Level Complete
After etch
After metal
After metal

## Slide 34: Completed Via Chains
34
M2
V2
M1

## Slide 35: Via Chain – 120 nm 1000 Contacts
Yield statistics (6 valid and identical chains tested)
  Overall yield of 1000-contact chains with via CD 120 nm (nominal) / 115 nm (final) – 96.83%
  Individual contact yield – 99.9968%
Template CD = 120 nm
Final CD = 115 nm
Cu (M2)
Coral
Cu (M1)
Ta

## Slide 36: 1957 TODAY
IBM’s 5 MB Drive
Toshiba’s 4 GB Drive

## Slide 38: Very Small Features required for New Hard Disk Drives
Lodder, J.C., Journal of Magnetism and Magnetic Materials, 2004. p. 1692-1697.
Electron Beam Lithography
Nanoimprint Lithography
http://nextbigfuture.com/2009/06/electron-beam-lithography.html
http://www.patrickcarlberg.dk/Lic/Intro%20mm/lith_image2.htm
http://www.itmweb.com/bimages/mitechnique.jpg

## Slide 39: Printing Bit Patterned Media
12nm Half Pitch Resist Pillars on Disk
From a hole tone template
-
BPM Disk Imprint
-
2.5
-
inch Disk
NuTera
TM
HD7000