## Slide 1
Lecture 14
Chemical Engineering for Micro/Nano Fabrication
Wafer
Wafer
Lamellae

## Slide 3: Very Small Features required for New Hard Disk Drives
Lodder, J.C., Journal of Magnetism and Magnetic Materials, 2004. p. 1692-1697.
Electron Beam Lithography
Nanoimprint Lithography
http://nextbigfuture.com/2009/06/electron-beam-lithography.html
http://www.patrickcarlberg.dk/Lic/Intro%20mm/lith_image2.htm
http://www.itmweb.com/bimages/mitechnique.jpg

## Slide 4: Printing Bit Patterned Media
12nm Half Pitch Resist Pillars on Disk
From a hole tone template
-
BPM Disk Imprint
-
2.5
-
inch Disk
NuTera
TM
HD7000

## Slide 5: Bad News….we cant make the templates!!
Takes ~ 1 month to write one template !!!
Cost ~ $ 106 / template
Master template
Electron Gun
Rotating Spindle Stage
Linear Stage
Template Mastering with Rotary E-beam
This is just far too Slow!!!
Notes: 5

## Slide 7: Polymers may offer the Miracle!!
Effect of annealing on blend morphology

## Slide 8: Miracle of Block Copolymers
Volume Fraction A
A
B
Notes: xN represents the driving force for phase separation
X – interaction parameter, represents energetic penalty of mixing components. Essentially like a solubility parameter

## Slide 9: Miracle process flow….. No optics
Substrate
Substrate
1. Spin coat BCP
2. anneal
3. Selectively etch one block
Substrate
10nm lines

## Slide 10
Ricardo Ruiz & Tom Albrecht
The Miracle of Block Copolymers
1X e-beam pattern
1/4X e-beam pattern
B
C
P
B
C
P

## Slide 11
Unfortunately…..not small enough!!!
Resolution limited by the block copolymer


## Slide 12: Resolution of PS-PMMA is limited to ca 22 nm by low c
Goal: Higher resolution than that of PS-PMMA
  High c ... gives small structures…
Incorporate Si in one block
  This gives high etch contrast
Amenable to orientation and alignment
No new unit processes required for Manufacturing
  No solvent annealing, no “SIS” processing
ACS Nano, 2015, 9 (7), pp 7506–7514
Poly[styrene-b-methyl methacrylate]
Polystyrene-b-poly(methyl methacrylate)

## Slide 13: We need high c and small N
Macromolecules 2006, 39, 2449-2451
Volume Fraction A
A
B
N
How to Shrink Block Copolymer Domains

## Slide 14: So…what is this c thing anyhow??
Flory Huggins Mixing Theory
here c, the “interaction parameter” describes the enthalpy change due to interspersing the two polymers. It is a function of variables including temperature…..
Polymer pairs with big c hate each other!!

## Slide 15: Design Criteria for New BCP
High c ... gives small structures
Incorporate Si in one block….. etch contrast
Amenable to orientation and alignment
No new Unit processes required for mfg

## Slide 16: Reactive Ion Etch Development
Maher et al. Chem. Mater. 2014, 26, 1471
Steve Sirard, Lam
Oxidizing Conditions
Si 10%

## Slide 18: Synthesis challenge → Anionic

## Slide 19
Anionic Polymerization
MeOH
Aliquot
Clear
 | Aliquot | BCP
Mn | 3,997 | 7,677
Mw | 4,261 | 7,924
PDI | 1.07 | 1.03

## Slide 20: Living anionic is effective but dangerous!

## Slide 21: Next….The Orientation Control Challenge
Wafer
Wafer
Lamellae
Bates et al. Science 338, 775 (2012)
Maher et al. Chem. Mater. 2014, 26, 1471

## Slide 22: Block Copolymer Orientation
Periodicity “L0” ~ 5-100 nm
Substrate
L0
Substrate
L0
Parallel
Perpendicular
AB diblock

## Slide 23
Wafer
Surface Prefers Red Block
1*L0
As cast film thickness > L0?
1.2*L0
2*L0
As-cast film thickness < L0?
Islands
1*L0
0.8*L0
Holes

## Slide 24: The “island and hole” experiment
Structures are easily seem by optical microscopy
Islands

## Slide 25
Wafer
Which Block Wets?
Incommensurate Initial
Film Thickness
1.2*L0
Wafer
Majority
1*L0
Red Wets
Islands
2*L0
Red Wets
Si is always on top!
1*L0
Wafer
Majority
1.5*L0
Blue Wets
Holes
0.5*L0
Blue Wets
Peters, R. D. et al., Langmuir 2000, 16, 4625.

## Slide 26: Thin film orientation
Air
Bang et al. Adv. Mater. 2007, 19, 4552

## Slide 27: Types of wetting
Red block prefers to interact with the air
Symmetric wetting
n*L0
Asymmetric wetting
(n+1/2)* L0
PS Preferential Surface
PTMSS Preferential Surface
Coulon et al., Macromolecules 1989, 22, 2581.
Russell et al., Macromolecules 1989, 22, 4600.
Coulon et al., J. Phys. (Paris) 1990, 51, 2801.

## Slide 28: Island / hole analysis
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 22.74 | 22.74 | 23.06 | 22.419 | 22.419 | 22.74 | 22.419 | 21.458 | 19.217 | 12.811 | 4.484 | 0.641 | 0 | 0 | 0.32 | 0.641 | 0.961 | 1.602 | 4.484 | 11.21 | 18.576 | 21.458 | 20.818 | 18.256 | 12.811 | 5.445 | 1.281 | 0.32 | 0 | 0 | 0 | 0 | 0 | 0.32 | 0.32 | 0.32 | 0.641 | 1.602 | 4.804 | 11.85 | 19.537 | 22.099 | 22.419 | 22.419 | 21.779 | 21.779 | 21.779 | 22.099 | 21.779 | 22.099 | 22.099
1 L0 Holes
Red block prefers to interact with the air
1.5 L0
PS Preferential Surface
PTMSS Preferential Surface
1.0 L0
1.2 L0
0.5 L0
Mansky et al., Macromolecules 1997, 30, 6810 , Huang et al., Macromolecules 1999, 32, 5299,. Peters et al., Langmuir 2000, 16, 4625.
5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 1.085 | 0 | 0 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 1.085 | 2.17 | 5.967 | 13.562 | 19.529 | 21.699 | 22.241 | 22.241 | 22.241 | 22.241 | 22.241 | 21.156 | 18.444 | 13.019 | 5.967 | 1.085 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 0.543
1 L0 Islands
Scale bars are 5 µm
100 nm

## Slide 29: Finding the neutral composition
Result:
Surface treatment:
Initial BCB thickness: 1.15 L0
Percent PtBuS:
Wafer
Neutral
0.5*L0
?
0.5 L0 Islands
PS and PTMSS wetting!
52%
65%
1 L0 Islands
PTMSS wetting
48%
1 L0 Holes
PS wetting
Scale bars are 5 µm
5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0.521 | 0.347 | 0.608 | 0.521 | 0.434 | 0 | 0 | 0.087 | 0.261 | 0.694 | 1.822 | 5.466 | 9.457 | 10.845 | 11.105 | 11.018 | 10.932 | 10.758 | 10.324 | 8.589 | 5.206 | 1.562 | 1.041 | 3.21 | 7.375 | 10.237 | 11.018 | 11.626 | 11.886 | 11.799 | 11.626 | 11.279 | 11.192 | 11.192 | 11.365 | 11.539 | 11.539 | 11.539 | 11.192 | 10.151 | 7.808 | 3.904 | 1.215 | 0.955 | 0.955 | 1.302 | 1.475 | 1.215 | 1.215 | 1.475 | 1.388

## Slide 30: Half L0 features on a neutral surface
1.25 L0
1.5 L0
Neutral Surface
1.0 L0
Neutral Surface
Scale bars are 5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 10.364 | 10.3103 | 10.5251 | 10.7399 | 11.1158 | 11.0621 | 10.5788 | 10.3103 | 9.7197 | 8.1087 | 4.9404 | 1.5573 | 0.5907 | 0.3222 | 0.3222 | 0.1611 | 0.0537 | 0.1074 | 0.3222 | 0.5907 | 0.5907 | 0.4833 | 0.4296 | 0.4833 | 0.4833 | 0.5907 | 0.5907 | 0.4296 | 0.3222 | 0.2148 | 0.2148 | 0.1611 | 0.2148 | 0.0537 | 0 | 0.3222 | 0.6981 | 0.8055 | 0.9129 | 1.8258 | 3.6516 | 7.1958 | 10.0955 | 10.901 | 10.8473 | 10.6325 | 10.6325 | 10.7936 | 11.0621 | 11.2769 | 11.1695
0.5 L0 Holes
1.35 L0
Kim et al. ACS Nano. 2013, 7, 9905.
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0.521 | 0.347 | 0.608 | 0.521 | 0.434 | 0 | 0 | 0.087 | 0.261 | 0.694 | 1.822 | 5.466 | 9.457 | 10.845 | 11.105 | 11.018 | 10.932 | 10.758 | 10.324 | 8.589 | 5.206 | 1.562 | 1.041 | 3.21 | 7.375 | 10.237 | 11.018 | 11.626 | 11.886 | 11.799 | 11.626 | 11.279 | 11.192 | 11.192 | 11.365 | 11.539 | 11.539 | 11.539 | 11.192 | 10.151 | 7.808 | 3.904 | 1.215 | 0.955 | 0.955 | 1.302 | 1.475 | 1.215 | 1.215 | 1.475 | 1.388
0.5 L0 Islands
1.17 L0
100 nm