## Slide 1
Lecture 15
Chemical Engineering for Micro/Nano Fabrication
100 nm

## Slide 2: Types of wetting
Red block prefers to interact with the air
Symmetric wetting
n*L0
Asymmetric wetting
(n+1/2)* L0
PS Preferential Surface
PTMSS Preferential Surface
Coulon et al., Macromolecules 1989, 22, 2581.
Russell et al., Macromolecules 1989, 22, 4600.
Coulon et al., J. Phys. (Paris) 1990, 51, 2801.

## Slide 3: Island / hole analysis
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 22.74 | 22.74 | 23.06 | 22.419 | 22.419 | 22.74 | 22.419 | 21.458 | 19.217 | 12.811 | 4.484 | 0.641 | 0 | 0 | 0.32 | 0.641 | 0.961 | 1.602 | 4.484 | 11.21 | 18.576 | 21.458 | 20.818 | 18.256 | 12.811 | 5.445 | 1.281 | 0.32 | 0 | 0 | 0 | 0 | 0 | 0.32 | 0.32 | 0.32 | 0.641 | 1.602 | 4.804 | 11.85 | 19.537 | 22.099 | 22.419 | 22.419 | 21.779 | 21.779 | 21.779 | 22.099 | 21.779 | 22.099 | 22.099
1 L0 Holes
Red block prefers to interact with the air
1.5 L0
PS Preferential Surface
PTMSS Preferential Surface
1.0 L0
1.2 L0
0.5 L0
Mansky et al., Macromolecules 1997, 30, 6810 , Huang et al., Macromolecules 1999, 32, 5299,. Peters et al., Langmuir 2000, 16, 4625.
5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 1.085 | 0 | 0 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 1.085 | 2.17 | 5.967 | 13.562 | 19.529 | 21.699 | 22.241 | 22.241 | 22.241 | 22.241 | 22.241 | 21.156 | 18.444 | 13.019 | 5.967 | 1.085 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 0.543 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 1.085 | 0.543
1 L0 Islands
Scale bars are 5 µm
100 nm

## Slide 4: Finding the neutral composition
Result:
Surface treatment:
Initial BCB thickness: 1.15 L0
Percent PtBuS:
Wafer
Neutral
0.5*L0
?
0.5 L0 Islands
PS and PTMSS wetting!
52%
65%
1 L0 Islands
PTMSS wetting
48%
1 L0 Holes
PS wetting
Scale bars are 5 µm
5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0.521 | 0.347 | 0.608 | 0.521 | 0.434 | 0 | 0 | 0.087 | 0.261 | 0.694 | 1.822 | 5.466 | 9.457 | 10.845 | 11.105 | 11.018 | 10.932 | 10.758 | 10.324 | 8.589 | 5.206 | 1.562 | 1.041 | 3.21 | 7.375 | 10.237 | 11.018 | 11.626 | 11.886 | 11.799 | 11.626 | 11.279 | 11.192 | 11.192 | 11.365 | 11.539 | 11.539 | 11.539 | 11.192 | 10.151 | 7.808 | 3.904 | 1.215 | 0.955 | 0.955 | 1.302 | 1.475 | 1.215 | 1.215 | 1.475 | 1.388

## Slide 5: Half L0 features on a neutral surface
1.25 L0
1.5 L0
Neutral Surface
1.0 L0
Neutral Surface
Scale bars are 5 µm
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 10.364 | 10.3103 | 10.5251 | 10.7399 | 11.1158 | 11.0621 | 10.5788 | 10.3103 | 9.7197 | 8.1087 | 4.9404 | 1.5573 | 0.5907 | 0.3222 | 0.3222 | 0.1611 | 0.0537 | 0.1074 | 0.3222 | 0.5907 | 0.5907 | 0.4833 | 0.4296 | 0.4833 | 0.4833 | 0.5907 | 0.5907 | 0.4296 | 0.3222 | 0.2148 | 0.2148 | 0.1611 | 0.2148 | 0.0537 | 0 | 0.3222 | 0.6981 | 0.8055 | 0.9129 | 1.8258 | 3.6516 | 7.1958 | 10.0955 | 10.901 | 10.8473 | 10.6325 | 10.6325 | 10.7936 | 11.0621 | 11.2769 | 11.1695
0.5 L0 Holes
1.35 L0
Kim et al. ACS Nano. 2013, 7, 9905.
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0.521 | 0.347 | 0.608 | 0.521 | 0.434 | 0 | 0 | 0.087 | 0.261 | 0.694 | 1.822 | 5.466 | 9.457 | 10.845 | 11.105 | 11.018 | 10.932 | 10.758 | 10.324 | 8.589 | 5.206 | 1.562 | 1.041 | 3.21 | 7.375 | 10.237 | 11.018 | 11.626 | 11.886 | 11.799 | 11.626 | 11.279 | 11.192 | 11.192 | 11.365 | 11.539 | 11.539 | 11.539 | 11.192 | 10.151 | 7.808 | 3.904 | 1.215 | 0.955 | 0.955 | 1.302 | 1.475 | 1.215 | 1.215 | 1.475 | 1.388
0.5 L0 Islands
1.17 L0
100 nm

## Slide 7: Top Interface Challenge
Not Soluble in H2O
Soluble in H2O
33
Ideal neutral surface
Polar solvent
solubility threshold
40

(mN/m)
72
25
H2O

## Slide 8: Top Coat Chemistry
1. Polarity switch
2. Tg greater than blocks
  PS = 105 ˚C
  PTMSS = 135˚C
3. Surface energy control
Requirements

## Slide 9: Top Coat Design
Mol fraction:
0.5
a + b = 0.5
a b
PTMSS Preferential
PS Preferential
Neutral

## Slide 10: Confined Island Hole test
1.2 L0
1.5 L0
1.0 L0
PS Preferential Surface
PS Preferential Surface
PS Preferential Top Coat
PTMSS Preferential Top Coat
5 µm
5 µm
Holes
Scale bars are 5 µm
Islands

## Slide 11: Confined island hole results for 22 nm diblock
LD 2-287
~ 1.40 L0
Initial BCP thickness: 1.19 L0
5 µm
5 µm
5 µm
5 µm
5 µm\
PS wetting
PTMSS wetting
PS wetting
PS wetting
5 µm
5 µm
5 µm
22 nm holes = 1 L0
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 21.133 | 20.863 | 20.594 | 20.325 | 19.787 | 19.248 | 17.768 | 13.864 | 6.865 | 1.211 | 0 | 0.269 | 0.673 | 0.942 | 0.807 | 0.404 | 0.269 | 0.807 | 3.769 | 10.364 | 17.498 | 20.594 | 21.536 | 21.806 | 21.94 | 21.806 | 21.671 | 20.863 | 19.114 | 14.672 | 7.268 | 1.884 | 0.942 | 0.942 | 1.077 | 1.077 | 1.211 | 2.019 | 4.98 | 11.441 | 18.306 | 20.998 | 21.402 | 21.267 | 20.998 | 20.46 | 20.19 | 20.325 | 20.19 | 20.19 | 20.594
49% di-tBuS
PS Wetting
All scale bars = 5 µm
Top Coat:
25% di-tBuS
12% di-tBuS
22 nm islands = 1 L0
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0 | 0 | 0 | 0.142 | 0.285 | 0.285 | 0.427 | 0.285 | 0.427 | 0.142 | 0.142 | 0 | 0 | 0.427 | 2.561 | 8.253 | 15.936 | 20.347 | 21.485 | 21.912 | 21.485 | 21.201 | 21.201 | 21.201 | 21.059 | 21.343 | 21.485 | 21.912 | 22.197 | 22.339 | 22.197 | 21.485 | 19.351 | 14.656 | 7.968 | 2.704 | 0.569 | 0.854 | 0.996 | 1.281 | 0.996 | 0.854 | 0.854 | 0.854 | 0.854 | 0.996 | 0.854 | 0.854 | 0.854 | 0.996 | 1.281
10 nm islands = 0.5 L0
Chart: x (µm)
| 0 | 9.8000000000000004E-2 | 0.1961 | 0.29409999999999997 | 0.39219999999999999 | 0.49020000000000002 | 0.58819999999999995 | 0.68630000000000002 | 0.7843 | 0.88239999999999996 | 0.98040000000000005 | 1.0784 | 1.1765000000000001 | 1.2745 | 1.3725000000000001 | 1.4705999999999999 | 1.5686 | 1.6667000000000001 | 1.7646999999999999 | 1.8627 | 1.9608000000000001 | 2.0588000000000002 | 2.1568999999999998 | 2.2549000000000001 | 2.352899999999976 | 2.4510000000000001 | 2.5489999999999999 | 2.6471 | 2.7450999999999999 | 2.8431000000000002 | 2.9411999999999998 | 3.0392000000000001 | 3.1373000000000002 | 3.2353000000000001 | 3.3332999999999999 | 3.4314 | 3.5293999999999999 | 3.6274999999999999 | 3.7254999999999998 | 3.8235000000000001 | 3.9216000000000002 | 4.0195999999999996 | 4.1175999999999746 | 4.2157 | 4.3136999999999999 | 4.4118000000000004 | 4.5098000000000003 | 4.6077999999999957 | 4.7058999999999997 | 4.8038999999999996 | 4.9020000000000001
 | 0.145 | 0.145 | 0.145 | 0.145 | 0.29 | 0.29 | 0.29 | 0.58 | 0.725 | 1.305 | 1.595 | 2.32 | 3.77 | 6.235 | 8.7 | 10.005 | 10.15 | 10.005 | 9.135 | 7.105 | 4.06 | 1.595 | 0.58 | 0.435 | 0.29 | 0.435 | 1.74 | 4.35 | 7.395 | 8.99 | 9.715 | 10.005 | 10.005 | 10.005 | 10.005 | 9.57 | 9.425 | 8.845 | 7.54 | 5.365 | 3.045 | 1.015 | 0.29 | 0.145 | 0 | 0 | 0.145 | 0.435 | 0.29 | 0.145 | 0
Notes: Figure SX: (a-d) Optical micrographs, (e-h) AFM height, and (i-l) AFM height traces of PS-b-PTMSS (L0 ≈ 22 nm) topography formed when confined between a top coat (12, 25, or 49% Pdi-tBu) and PS substrate surface treatment and annealed at 180°C for 6 min. Scale bars represent 5 µm.

## Slide 12: Orientation Results
Neutral Interfaces
PS Preferential Interfaces
PTMSS Preferential Interfaces
Maher et al. Chem. Mater. 2014, 26, 1471 All scale bars = 200 nm
1.0 L0
1.5 L0
2.0 L0
2.3 L0
3.0 L0
BCP on
neutral surface
Apply top coat
Anneal
L0
Etch

## Slide 13: The Search for c
c
c

## Slide 14
Chart: q (nm-1)
Chart: 1/T
| 2.4204284158296022E-3 | 2.3086690522913541E-3 | 2.2067747986317999E-3 | 2.1134946634259748E-3
 | 0.047444 | 0.047302 | 0.047129 | 0.047002
Rheology is also a valuable tool for determination of c
Durand, et. al Journal of Polymer Sci., 2014
Determine χ by SAXS

## Slide 15
193 ֯C
224 ֯C
167 ֯C
BCP | PDSS-PMDOS | PDSS-b-P2VP
χ (T) |  | 
χ (180C) | 0.102 | 0.123
BCP | PDSS-PMDOS | PDSS-b-P2VP
χ (T) |  | 
χ (180C) | 0.102 | 0.123
Determine χ by Rheology
χNODT = 10.5
χ(T) = + b
= + b
11

## Slide 16: Increasing c
0.045
0.048
0.11
0.14
0.23
PS-b-PMMA

## Slide 17: Oriented high c block copolymers
40 Angstrom lines
50 Angstrom lines

## Slide 18
q=0.00590  10.6 nm
50 Angstrom Lines and Spaces
Small Structure for Bit Patterned Media

## Slide 19: Image Transfer of 50 Å lines and Spaces
Spin-on carbon (15 nm)
Silicon wafer
Chromium (4 nm)
BCP mask + Neutral brush (8 nm)
BCP etch (CO2 RIE)
Cr/SOC etch (Cl2/O2 RIE)
Scale bar = 100 nm

## Slide 20: Now…Alignment Control - DSA
Nealey, Russell, Ross, et al
Directed Self Assembly

## Slide 21: Can we orient these high c materials
Even Nature struggles with this Challenge

## Slide 22: A “Hybrid” process flow created to incorporate top coat and combine chemical and topographic anchoring for DSA
Chemistry of brush:
Chemistry of XST
Chemistry of ~20 nm BCP:
Chemistry of TC:
Blachut, G., et al. Chem. Mater (2016), 28(24), 8951-8961.

## Slide 23: Design for n=4 & 0.5Lo where Lo =20
40nm lines and spaces
Line is subsequently “trim etched” to 10nm
Challenging Lithography
This is the theoretical limit for 193nm immersion litho
Top coat should be perfectly neutral
Brush approaches neutral with increasing multiplication
Guide line should strongly favor one block

## Slide 24: Directed Assembly at HGST Electron Beam written Guide patterns
ACS Appl. Mater. Interfaces 2015, 7, 13476
10 nm Lines and spaces
Julie
Ricardo

## Slide 25: Greg in Belgium!
PMOST-PTMSS
Gregory Blachut
200nm
L0 = 19.7 nm
Chem. Mater 28(24)8951-8961 (2016)