## Slide 1
Lecture 16
Chemical Engineering for Micro/Nano Fabrication
Oskar Süẞ (Suess)

## Slide 3: Guide line by 193 Immersion and trim etch

## Slide 4: Greg in Belgium!
PMOST-PTMSS
Gregory Blachut
200nm
L0 = 19.7 nm
Chem. Mater 28(24)8951-8961 (2016)

## Slide 5: Directed Assembly at HGST Electron Beam written Guide patterns
ACS Appl. Mater. Interfaces 2015, 7, 13476
10 nm Lines and spaces
Julie
Ricardo

## Slide 6: Design for n=4 & 0.5Lo where Lo =20
40nm lines and spaces
Line is subsequently “trim etched” to 10nm
Challenging Lithography
This is the theoretical limit for 193nm immersion litho
Top coat should be perfectly neutral
Brush approaches neutral with increasing multiplication
Guide line should strongly favor one block

## Slide 7: Possible Interpretation of Imec Cross sections
TEM/EELS of Cross section
Score: 178K
23 ± 1 nm

## Slide 8: Relaxed Optical Litho Proposal Design for n=4, Lo = 20
80nm
80nm
Top coat and XST should be perfectly neutral for all n
Polar oxidized sidewall
Requires selective reaction of the brush with substrate not sidewall !!

## Slide 9: 5 nm DSA using Imprint Lithography
Anneal
190˚C
2 min
Wafer
Imprint
Resist
Selective
brush graft
to Chromium
Brush
O2 RIE
Chromium
Apply BCP
Apply TC
Top Coat
BCP
develop TC

## Slide 10
50 Å lines and spaces
Notes: To start things off, I’d just like to show you the final result of our hard work at Seagate. What you see here is a top-down SEM of aligned BCP lamellae. Each of these lines is 5 nm wide. We are particularly proud of this result because we don’t think DSA has ever been done before using features this small, although people are getting close. From Seagate’s perspective, they would like to take each of these lines defined by the block copolymer and chop them up into small rectangles, and that process can eventually be done using a variety of methods. As rectangles, they would be useful in defining the individual bits, the 1s and 0s in a hard disk drive. The technology of inidividually patterning bits like this is known as bit patterned media, and it is being investigated because it offers HDD manufacturers to scale storage density to something like 5 Tb/in^2 of data, maybe more.

## Slide 11
(Map contrasts are optimized to show element distributions, they are not directly proportional to actual abundances)b
C-Si-Cr
Elemental Overlay Map
Looks great from the top!!

## Slide 12: STEM Cross sections of Latest 5nm Process

## Slide 13
collaboration with
Etch developed 50 Å lines and spaces

## Slide 15: Back to Resists

## Slide 16
Recall
KTFR

## Slide 17: Blue Print Chemistry

## Slide 20
Meyer
Baekeland
The History of Novolac
C.H. Meyer and L.H. Baekeland Discovered Novolac ca. 1900

## Slide 22
Novolac Resin Production!!
Workers at Albert Co. in Wiesbaden, Germany
“zerkleinert das Harz von Hand” (ca. 1910)

## Slide 23
Oskar Süẞ
Der Diazo König

## Slide 25
Novolac/DNQ Photoresists
Develop
Inhibited Novolac (I)
LogR
Novolac
UV
Coat
Expose
Substrate
I
I
I
I
I
I
I
I
I
I
I
I
Substrate
I
I
I
I
I
I
I
I
P
P
P
P
P
P
Substrate
I
I
I
I
I
I
I
I
UV
Photoproduct (P)
365-nm exposure
Add DNQ
I
P
Notes: The first example -- Diazonaphthoquinone/Novolac chemistry.
These photoresists operate by taking the base soluble polymer, novolac and adding a small amount of a photoactive dissolution inhibitor, diazonaphthoquinone.
Adding the DNQ causes the dissolution rate of the resist to decrease by several orders of magnitude.
The DNQ acts as the photochemically solubility switch, such that upon exposure to 365 nm light, it’s converted to a carboxylic acid.
And this exposed resist has a higher dissolution rate than the novolac alone.
The result of this change in dissolution rate is a resist image with a nearly vertical sidewall profile.
Looking at this, you’d think that the perfect resist already exists .. And it does ... Unless you want to decrease the size of the image.

## Slide 26
DNQ – Novolac Resists

## Slide 27
Wolff Rearrangement and Reaction of the ketene with water