## Slide 1
Lecture 18
Chemical Engineering for Micro/Nano Fabrication

## Slide 4
Effect of Humidity on Dissolution Rate

## Slide 5
Dissolution Rate vs Post Apply Bake Temperature

## Slide 7
Negative Resist Characterization

## Slide 9
Simulated Electron Beam Exposure

## Slide 13
Radiation Induced Decomposition
of Poly(methyl methacrylate), PMMA

## Slide 15
Measuring “G” Values

## Slide 16
“G” Values

## Slide 17
RESIST SENSITIVITY EXPRESSED IN TERMS OF DOSE/UNIT
AREA IS LIKE AN EPA MILEAGE RATING… USE IT FOR
COMPARISON ONLY. YOUR OWN MILEAGE WILL VARY
DEPENDING ON…
Lithographic Sensitivity
CAUTION…

## Slide 18: Defocus Behavior: a 193 nm Resist
100nm (1:1.1) Trench DOF @
38.0 mJ/cm
²
-
0.05µm
-
0.10µm
-
0.15µm
-
0.2µm
-
0.25µm
-
0.35µm
0.0µm
+0.05µm
+0.10µm
-
0.30µm
+0.15µm
+0.2µm
+0.25µm
+0.30µm
+0.35µm
+0.4µm
+0.20µm
+0.10µm
+0.35µm
+ 0.
05
µm
120
à
100
nm Isolated Trench
+0.30µm
-
0.
1
0µm
0.00µm
-
0.
1
5µm
180
à
100nm
Isolated LINE
0.110µm
0.110µm
0.109µm
0.111µm
0.111µm
0.107µm
0..113µm
+0.
10
µm
+0.
0
5µm
0.
0
µm
+0.20µm
-
0.
1
0µm
-
0.05µm
-
0. 15µm
+0.4
0
µm
+0.35µm
+0.45µm
-
0.40µm
0.114µm
0.114µm
0.112µm
0.112µm
0.116um
0.116µm
0.112µm
0.115um
0.115µm
0.114µm
0.116µm
0.117µm
0.115um
0.112µm
0.115µm
0.116um
-
0.05µm
Exactly what does this measure???