## Slide 1: Lecture 2
Chemical Engineering for Micro/Nano Fabrication

## Slide 2
Rubylith Mask Making

## Slide 3: Rubylith Mask Making

## Slide 4
Masks Making
Earliest Masks were “emulsion” Masks made by photographic processing
  Emulsion Masks were made on glass
  This design failed due to fragile character of the gelatin emulsion
The emulsion Mask was replaced with Chromium on glass
  This fundamental design has persisted to this day
We will discuss the fabrication of modern masks in some detail later in the course.

## Slide 5: Photographic emulsion of AgCl
Expose
Fix – Sodium Thiosulfate
Develop - monomethyl-p-aminophenol hemisulfate, base
Stop – Acetic Acid

## Slide 6
Engineering Drafting

## Slide 7
CAD Drawn Mask

## Slide 8: Laser Mask Writers

## Slide 9: Laser Mask Writers

## Slide 10
Electron Beam Lithography

## Slide 11: Electron Beam Lithography for Masks
Converts Computer patterns into Masks
High resolution but slow and very expensive!

## Slide 12: Toppan Photomask Round Rock, TX

## Slide 13: Contact Mask Aligner

## Slide 14
Contact Mask Aligner

## Slide 15: We Started With Contact Printing
Spherical
Mirror
Element of
the Condenser
Point
Source
Mirror
Heat Removing Filter
Wafer
Element of
the Condenser
Shutter
Z-movement
Mask
Swiveling
movement
X-movement
Resist
Notes: The light source is usually a point source, typically a gas discharge arc lamp such as Xenon (Xe), or Mercury (Hg) arc lamps chosen for high efficiency in the desired spectral region.
The photomask is pressed against the wafer with a pressure of 0.05 – 0.3Atm.
Advantage: The mask contains all the patterns for all of the chips on the wafer. So every pattern is exposed in a single exposure.
How good is the technique?

## Slide 16
100%
INFORMATION
MASK
WAFER
The Fundamental Issue – Information Transfer
Light Source
OPTICAL
LITHOGRAPHY
SYSTEM
LESS THAN 100% INFORMATION
Notes: Resolution relates to how fine a feature, such as a line or trench, can be reproduced in the resist from the aerial image. It is related to the optical contrast of the resist, which is determined by the resist chemistry and by processing.
Recall that I did not draw the aerial image in the previous slide as a square wave, which would correspond to the IDEAL light intensity distribution at the wafer plane . Rather I showed the intensity distribution at the wafer plane as a GAUSSIAN-type distribution, which gives rise to a corresponding Gaussian distribution of absorbed energy density in the resist.
Clearly the fidelity of the aerial image has been degraded by the exposure tool. If the square wave pattern associated with the mask represents 100% information then the transmitted aerial image clearly represents less than 100% information.
The problem is that the line edge of the aerial image of the feature is difficult to determine. The design of the resist can compensate to some degree for this loss in image fidelity, but clearly the closer the aerial image is to the ideal light intensity pattern square wave, i.e., the higher the optical contrast, the easier it should be in principle to realize the desired critical dimensions in the resist.
Hence it is important to understand what factors control the quality of the aerial image and how they can be manipulated to get the most out of the optical lithography system.

## Slide 17
MASK
LIGHT
Imax
Imin
Imax – Imin
Imax + Imin
MODULATION =
Glass
Chrome
Imax
Imax
Imin
Notes: Modulation is also known as OPTICAL CONTRAST

## Slide 18
ILLUMINATION
MASK
WAFER
RESIST
Modulation of the mask is ?
Modulation of the image is ?
Modulation in Contact Printing
1
~1
The image is almost perfect!
Imax – Imin
Imax + Imin
MODULATION =
Notes: Problem is that the mechanical contact between the mask and wafer causes defects on the mask and wafer with consequent negative impact on productivity.

## Slide 19: But….let’s look at some Resists

## Slide 20
“It” All Started Here
NICÉPHORE
NIÉPCE
1765-1883

## Slide 21
Chalone sur Soane

## Slide 22
A Historical Perspective
“Point de vue du Gras” by Nicephore Niepce
Printed with Bitumen of Judea 1826

## Slide 23
Contact Printing in Bitumen of Judea
A Contact Photogravure
of Cardinal d’ Amboise
by Niepce (1826)

## Slide 24
PMMA in MIBK

## Slide 25
Dicromated Gelatin
William Henry Fox Talbot
Photographed in 1864
Protein + K2Cr2O7
High Sensitivity
Poor Shelf Life

## Slide 26
Early Planar Integrated Circuit
Shockley Noyce Ca. 1960

## Slide 27
The First Synthetic Photopolymer
Louis Minsk
Eastman Kodak
Poly(vinyl cinnamate)
Adhesion Problems

## Slide 28
Co-inventors of Kodak’s KTFR
Martin Hapher Hans Wagner

## Slide 31
This stuff is GLUE!!

## Slide 32
It cannot sustain high aspect ration images.
Swelling, Snakes, Ugh!!