## Slide 1: Lecture 20
Chemical Engineering for Micro/Nano Fabrication

## Slide 2
Exam II
When: 9:30- 11 AM Thursday Nov. 15th
Where: FNT 1.206A
What: Lectures through 11/14/2018
Bring: Pencil and eraser
Do: Study notes, review quizes and ask questions…work with a friend??

## Slide 3
Photochemistry Counts Photons
Starting Material + Photon Product
Energy/Photon, E = hv = hc/
As Wavelength Decreases, Energy/Photon Increases
Fewer photons are available for a given exposure
measured in millijoules/area
Mercury lamp produces far less Energy in the
Deep UV
Throughput Therefore Requires
-- Brighter Light Bulbs
-- More Sensitive Resists

## Slide 4
Control of Resist Sensitivity

## Slide 5
Excimer Lasers are very bright “lights”

## Slide 6
Noble gases do not usually form chemical compounds. However, when in an excited state (induced by electrical discharge), they can form temporarily bound molecules with themselves (excimer) or with halogens (exciplex) such as fluorine and chlorine. The excited compound can release its excess energy by undergoing emission, resulting in a strongly repulsive ground state molecule which very quickly dissociates back into two unbound atoms.
Excimer / Exciplex Lasers

## Slide 8
An Excimer Laser

## Slide 9
Excimer Lasers

## Slide 10
First Excimer Laser Lithography Experiment
Reciprocity proof!!

## Slide 11
Insoluble
hn
Soluble
F < 1
Generator
hn
F < 1
Catalyst
Insoluble
Soluble + Catalyst
Chemical Amplification

## Slide 12
Anionic polymerization of Phthalaldehyde

## Slide 13
For reversible polymerizations, there is a temperature where the position of the monomer / polymer concentration is at equilibrium, where ΔG = 0.
at equilibrium ΔG = 0 = ΔH - T ΔS
or, the Ceiling Temperture, Tc = ΔH / ΔS
Ceiling Temperature, Tc
α-methylstyrene | 66 | 
styrene | 395 | 
Tc °C

## Slide 14
Photoacid Generation Mechanism
of Aryl Sulfonium Salts
Dektar, J. L.; Hacker, N. P. J. Am. Chem. Soc. 1990, 112, 6004.

## Slide 15
Thermogravimetric analysis of PAGs

## Slide 16
Optical Micrographs of “self-developed” Images in Polyphthalaldehyde

## Slide 17: Chemically Amplified Deep UV Resists
Photoacid Generation
Acid-Catalyzed Deprotection
S+-SbF6
h
H+-SbF6
CH2
CH
O
O
O
n
H+
CH2
CH
OH
n
+
CO2
+
CH2=C
CH3
CH3
+
H+
100
150
200
300
250
Temperature (°C)
Mass
with
acid
without
acid
D
protecting
group

## Slide 18
Absorbance

## Slide 20
Infrared analysis

## Slide 21
ROX level of 1M DRAM IBM
First Commercial Implementation of Deep UV Photolithography

## Slide 22
T-BOC line-width dose response
Negative tone development

## Slide 23
sample structures

## Slide 24
Another approach

## Slide 25
High And Low Activation Energy Protective Groups
O
H
O
O
n
n
N
O
O
O
O
n
O
H
O
R’
O
R
O
O
R
R
'
n
O
H
C
H
3
O
O
acetal
n
n
t-butyl
ester/ether,
sec. alkyl
low Ea
high Ea

## Slide 26: The Skeleton in the Closet

## Slide 29
t-BOC Resist in negative tone
- anisole developer
15 ppb of N,N-dimethylaniline

## Slide 30
15 min in filtered air
15 min in 10ppb NMP before exposure
“T” tops
NMP

## Slide 31
No Delay Post Coating Delay

## Slide 32
W. Hinsberg, IBM
Polymer Permeability

## Slide 33
W.D. Hinsberg, et.al. IBM, Almaden

## Slide 38
Hiroshi Ito, IBM
Thermogravimetric analysis

## Slide 40
Effects of filtered air (top) and 10ppb NMP (bottom) on positive images printed in the meta- (left) and para- (right) P(HOST-co-BOCST) resists.

## Slide 42
The “Family”

## Slide 43: ESCAP
Acrylic reduces solubility of NMP
Acrylic ester more thermally stable than the t-butyl carbonate
Enables post apply bake Temp > Tg
Bake > Tg decreases permeance
Hiroshi Ito, IBM

## Slide 44: IBM Mainframe Circuit Board
one of 20 layers printed circuit board that contained nearly a mile of wire interconnections used in IBM Mainframes.

## Slide 45: SU-8 Negative Resist

## Slide 46: IBM CGR Negative Resist
PAG

## Slide 49
Entergris, Inc
Air purification system