## Slide 1: Lecture 21
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Snoods??..Beards???..Wattles??
http://mentalfloss.com/article/53730/whats-thing-hangs-turkeys-face
https://tpwmagazine.com/archive/2005/nov/skillbuilder/

## Slide 3
Relative Etch Rate of Polymers
Relative Etch Rate
Aliphatic
Aromatic

## Slide 4
Insoluble
hn
Soluble
F < 1
Generator
hn
F < 1
Catalyst
Insoluble
Soluble + Catalyst
Chemical Amplification

## Slide 5: Chemically Amplified Deep UV Resists
Photoacid Generation
Acid-Catalyzed Deprotection
S+-SbF6
h
H+-SbF6
CH2
CH
O
O
O
n
H+
CH2
CH
OH
n
+
CO2
+
CH2=C
CH3
CH3
+
H+
100
150
200
300
250
Temperature (°C)
Mass
with
acid
without
acid
D
protecting
group

## Slide 6: Design Considerations
Dissolution by etching prevents swelling
Incorporates Catalysis to achieve high sensitivity
Employs polyphotolysis for high contrast
Can be developed in either tone
High transparency for steep walls.
Aromatic polymer provides dry etch resistance
High activation energy provides storage stability

## Slide 7
Absorbance
Optical Density

## Slide 8: Remember the Skeleton in the Closet

## Slide 11
Effects of filtered air (top) and 10ppb NMP (bottom) on positive images printed in the meta- (left) and para- (right) P(HOST-co-BOCST) resists.

## Slide 12
The “Family”

## Slide 14: ESCAP
Acrylic reduces solubility of NMP
Acrylic ester more thermally stable than the t-butyl carbonate
Enables post apply bake Temp > Tg
Bake > Tg decreases permeance
Hiroshi Ito, IBM

## Slide 15
Next: 193nm Lithography

## Slide 16
Relative Etch Rate of Polymers
Relative Etch Rate
Aliphatic
Aromatic

## Slide 17
The Ohnishi Number
Watanabe, F. and Ohnishi, Y., J. Vac. Soc. Technol. B,422 (1986)

## Slide 18
Meta-cresol novolak
Poly-(4-hydroxystyrene)
Polyacrylates
(aliphatic)
200
225
250
275
300
325
375
350
400
175
0.4
0.8
1.2
1.6
2.0
2.4
2.8
0.0
Wavelength [nm]
Absorption coefficient [1/µm]
ArF
193 nm
KrF
248 nm
i-line
365 nm
Source: R.D. Allen et al., IBM J. Res. Develop. 41 (1/2), 95-104 (1997)
Absorption of Photoresist Polymers

## Slide 19
Relative Etch Rate of Polymers
Relative Etch Rate
Aliphatic
Aromatic
Carbon

## Slide 20
248 and 365 nm resists are unsuitable for 193 nm imaging because they are opaque at this wavelenth
Etch resistance requires high carbon/hydrogen ratio but aromatics are precluded because of their absorption
How do you achieve both 193nm optical transparency and etch resistance?
193 nm Resist Materials
Challenge:

## Slide 21
High C:H Ratio of Alicyclic Hydrocarbons
Structure:
Formula:
Unsaturation
Number:
The key!

## Slide 22: APEX 248nm Resist Design
Tethering Function
Acid Lability
Base Solubility
Etch Resistance

## Slide 23
UTexas193nm Design
Tethering Function
Etch Resistance
Acid Lability
Base Solubility
C
O
O
C
O
C(CH3)3
OH
[
[
]
]

## Slide 24
Early Lithography
Excellent image quality
Adhesion failure
Resist
+ Ø3SSbF6
poly(NBCA-co-CBN)
Synthesis requires metal catalyst!

## Slide 25
Trading Etch Resistance for Adhesion:
Alternating Systems: COMA
Yield :
Mn :
Mw :
Pd :
60%
4,660
6,860
1.472
Waco Chemical
No Metal!
V601
Shelf Life issues?

## Slide 26
Images in UT 193nm COMA Resist
Alternating co-polymer
Uzo Okoroanyanwu, Jeff Byers

## Slide 27
Improving Etch Resistance
UV Absorbance
0.44 mm-1
@ 193 nm
Yield :
Mn :
Mw :
Pd :
55 %
3,400
4,340
1.276
DNBC
With JSR

## Slide 28: Resist and Process Development
I-line
248nm
193nm Issues!
Basic
Chemistry
Formulation and Process Development
Optimization
Performance
Time

## Slide 29: Fujitsu’s Acrylic Platform
Acrylate Copolymers …
Free radical polymerizations
No metal

## Slide 30: Acrylic Polymer Platform
Fujitsu
IBM,JSR, etc.

## Slide 31: Types of PAGs Used For 193 nm Lithography
A
sF
6
-
P
F
6
-
R
f
S
O
3
-
F
3
C
S
O
3
-
S
O
3
-
S
+
O
C
H
3
N
O
O
O
S
O
O
A
r
N
O
O
O
S
O
O
C
F
3
F
3
C
C
F
2
C
F
2
C
F
2
S
O
3
-
NEALS
I
+
S
+
DPI
TPS
R
R
R
R
IONIC
VOLATILE
NON-VOLATILE
: too weak
for 193 nm
NON-IONIC
O
O
H
O
S
O
O
N
O
O
O
S
O
O
C
F
3
MBT
NIT
MDT
SIT
“nonaflate”
O
S
O3-
ALS
NAT.OTf
S
+
O
C
H
3

## Slide 32: 193nm Resist Challenges
Pattern Collapse
Line Edge Roughness (LER)
Etch Resistance
Heisenberg Principle issue
New Defect Types
Pattern Collapse
LER
m Bridging