## Slide 1: Lecture 22
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Final Exam
When: Thursday December 13th from 9:00 am – Noon
Where: ETC 2.114
Bring Pencil, eraser....no calculator.
Corrected Exams will be available for you in NHB 5.136 after the grades are posted.

## Slide 3: What to Review
Quizes
Midterm exams
Graduate Presentations
Vocabulary and acronym list
Extract basic principles from notes
  Relationships that connect variables such as wave length, slit width, gap, etc with resolution energy/photon, etc.
  What caused the “abandoned” processes to fail?
    What was learned from this??
  How do the various photoresist systems work?
What are the current strategies for manufacturing and what are the challenges with these technologies?
Study with a friend
Write a test
Come to visit and ask questions!!

## Slide 4: Chemically Amplified Deep UV Resists
Photoacid Generation
Acid-Catalyzed Deprotection
S+-SbF6
h
H+-SbF6
CH2
CH
O
O
O
n
H+
CH2
CH
OH
n
+
CO2
+
CH2=C
CH3
CH3
+
H+
100
150
200
300
250
Temperature (°C)
Mass
with
acid
without
acid
D
protecting
group

## Slide 5: 248 nm Resist Design Considerations
Dissolution by etching prevents swelling
Incorporates catalysis to achieve high sensitivity
Employs polyphotolysis for high contrast
Can be developed in either tone
High transparency for steep walls.
Aromatic polymer provides dry etch resistance
High activation energy provides storage stability

## Slide 6
The “Family” of DUV Resists

## Slide 8
The Ohnishi Number
Watanabe, F. and Ohnishi, Y., J. Vac. Soc. Technol. B,422 (1986)

## Slide 9: Resist and Process Development
Basic
Chemistry
Formulation and Process Development
Optimization
Performance
Time

## Slide 10: Fujitsu’s Acrylic Platform
Acrylate Copolymers …
Free radical polymerizations
No metal

## Slide 11: 193nm Resist Challenges
Pattern Collapse
Line Edge Roughness (LER)
Etch Resistance
Heisenberg Principle issue
New Defect Types
Pattern Collapse
LER
m Bridging

## Slide 12: Line edge Roughness
193
248

## Slide 13: Intrinsic limitation?
Exposure
PEB
mask
Generation of chemically stable catalyst
hn
Solubility-switching
plus transport
Diffusion Bias sets the limit at ~ 30-50nm

## Slide 14
Acid Feeder Layer
Acid Detector Layer
FTIR
Bake Plate
Normalized FTIR
Peak at 1760 cm-1
+t
Mirror-backed Si wafer
The Sandwich Experiment
To test

## Slide 15
Initial PHOST Trilayer Experiments (~ 100 ºC)
Acid
Control
24 hrs
Many, many variations on this experiment were tried with similar results

## Slide 16
Nonaflic Acid Transit Time through 150nm PEMA vs. Temperature
0
10000
20000
30000
40000
50
55
60
65
70
75
80
85
90
95
100
Temperature (ºC)
Transit Time (seconds)
Glass Transition Region
Temperature Dependence of Diffusion in a Polymer Film
Tg = 70 ºC
D  L2/t

## Slide 17
D = 3x10-4 mm2/s
Fickian Diffusion Above Polymer Tg

## Slide 18
Acid Diffusion in PHOST
T (Cº)
*Values For Nonaflic Acid in PHOST
D (mm2/s)
Method
185
180
170
175
165
150
140
Summary Table*
extrapolation
extrapolation!
direct measure
direct measure
direct measure
direct measure
direct measure
1.0 x10-3
2.6 x10-5
2.6 x10-4
8.7 x10-5
6.5 x10-6
1.6 x10-7
1.3 x10-8
Transit Time vs Tbake
Tg = 170 ºC

## Slide 19
Reaction Front Propagation Hypothesis
- Active (mobile) acid molecules
- Inactive (immobile) acid molecules
High acid concentration region
Reaction zone
Reacted region (Bias region)
Unreacted region
Ignition of Reaction Front
Gradual Depletion of Front
Initial Condition

## Slide 20
UV
…it can be seen that the bilayer structure is just a rotated, isolated sidewall
Bilayer Experiment’s relations to the Sidewall
Exposure creats a latent image of photgenerated acid
Acid diffuses from exposed into unexposed regions
and everything outside the dotted box is ignored…
…If a sidewall is isolated and the wafer is rotated 90o…

## Slide 21
Acid Feeder Layer
Acid Detector Layer
FTIR
Bake Plate
Normalized FTIR
Peak at 1760 cm-1
+t
Mirror-backed Si wafer
The t-BOC Bilayer Experiment
Unexposed
Unexposed
Exposed

## Slide 22: SEM of bilayer interface
SEM was used to investigate the interface between the acid feeder and acid detector layers after a 35 minute bake.
The reacted region appears as a well-defined intermediate layer between the original two layers.
(Stewart et al., Proc. SPIE, 2000)
Tbake = 60 °C
130 nm
Tbake = 75 °C
230 nm
Tbake = 90 °C
415 nm
ACID DETECTOR LAYER
ACID FEEDER LAYER
INTERMEDIATE LAYER

## Slide 23: 3. SEM of bilayer interface: control experiment
Two bilayer samples were prepared identically, except that one was exposed with UV light and the other was unexposed.
The unexposed sample (no acid) has a distinct interface between the two layers, while the exposed sample has formed an intermediate layer.
Without Acid
With Acid
(Stewart et al., Proc. SPIE, 2000)
Detector Layer
Feeder Layer
Intermediate
Layer

## Slide 24
Bilayer Experimental Results
Slow Diffusion Region
Fast Diffusion Region
Bias

## Slide 25
Bilayer Experiments
75º C
90 ºC
100 ºC
110 ºC
Bias

## Slide 26: Effect of Counterion Size on Bias
~15nm

## Slide 27
Monte Carlo Lattice Modeling
2. Exposure
(Ch. 4)
1. Film Creation
(Ch. 2 & 3)
3. Post Exposure Bake
(Ch. 5)
4. Develop
(Ch. 6 & Appendix)

## Slide 28
Mesoscale Monte Carlo simulation
Resist components are represented as cells in a three dimensional lattice.
Polymer molecules are represented as a string of cells, where each cell represents a repeat unit.
Other lattice cells contain PAG, photoproducts, solvent, free volume, etc.
Each type of cell behaves differently in accordance with its chemical identity during a dynamic Monte Carlo simulation.

## Slide 29
Post Exposure Bake: Reaction and Shrinkage
Experimental results
Single layer photoresist film:
Reaction progress and film thickness are tracked simultaneously.
(Burns, Schmid et al., Proc. Int. Conf. on Photopolymers, 2000)
Preliminary simulation results
Simulation Time
FTIR
BAKE PLATE
ELLIPSOMETRY

## Slide 30: Influence of Base on LER
x
I(x)
Base
Acid
No base
With base
J. E. Meiring, T. B. Michaelson, G. M. Schmid and C. G. Willson, Proc. SPIE, 5753(2005), to be published
Base quencher can decrease the acid sphere of influence in low contrast regions, thereby reducing LER.

## Slide 31: Exploring Base Effects
I(x)
x
x
x
J. E. Meiring, T. B. Michaelson, G. M. Schmid and C. G. Willson, Proc. SPIE, 5753(2005), to be published
To add base quencher seems to make the contrast higher, thereby LER reducing.
0% base
15% base
30% base
6.61 nm RMS
5.47 nm RMS
3.89 nm RMS

## Slide 32
The good news is:
Intrinsic bias can be reduced by adding base
The bad news is:
a) This reduces the resist sensitivity very much

## Slide 33: The Big Trade Off