## Slide 1: Lecture 23
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Final Exam
When: Thursday December 13th from 9:00 am – Noon
Where: ETC 2.114
Bring Pencil, eraser....no calculator.
Corrected Exams will be available for you in NHB 5.136 after the grades are posted.

## Slide 3: The Big LER Trade Off

## Slide 4
Typical KrF system always shows moderate variation of DR……
0< DR @ Unexposed area
Gradually increasing DR
Low contrast value
Moderate Rmax
Uniform DR inside film
Typical ArF system always shows dramatic variation of DR……
No DR @ Unexposed area
No DR changes until this point
Suddenly the dissolution begins
The contrast is very high
Quite high Rmax
Different DR inside film
Comparison of ArF and KrF
Notes: I will try to introduce the difference between KrF and ArF about dissolution behavior. Here is Dissolution rate variation of KrF. Normally, they have dissolution rate, more than zero, and the dissolution rate is accelerated by exposure. The contrast is low. The Rmax is not so high, and the dissolution rate in side film is unfirom. On the other hand, here is the ArF’s. they don’t have any dissolution rate at unexposed area, No dissolution rate changes until this point. And then the dissolution is suddenly coming, the contrast is too high. The Rmax is quite high, and the dissolution rate in side film is not uniform.

## Slide 5: Dissolution behavior
DR
KrF System
ArF System
This difference in the contrast amplifies small variations in the blend region. “Digital” On/Off switching phenomenon makes the line edge rough.
Notes: OK. I will try to show my image of dissolution behavior of KrF and ArF resists. For KrF, half components are phenol. So they have dissolution rate at unexposed area. And then, generating carboxylic acid accelerates dissolution rate faster. Finally, the rate reaches Rmax. On the other hand, for ArF, most of components are lactone, and no dissolution rate. Even though COOH generates a little, lactone doesn’t contribute to DR because it’s not sufficient to open ring. And then suddenly the switch turns on, dissolution begins, reaches Rmax. So this different in the contrast amplifies small variations in the blend region.

## Slide 6: Is there such a thing as too much contrast?
The ArF system changes from insoluble to soluble over a very narrow dose range
Small fluctuations are amplified and cause huge changes in dissolution rate.
Stochastic process noise becomes line edge roughness
The KrF system has lower contrast
Small fluctiuations cause small changes in dissolution rate..
DR
Notes: The dissolution of KrF is analog like. The deprotection accelerates the DR, but the acceleration might not amplify small variations. On the other hand, ArF’s is digital like. The enough deprotection is required, and the dissolution occurs suddenly. The dissolution might amplify small variations. So as my speculations, LER reducing may require a polymer which has some dark film loss, like Phenol. That structure developed for 157 might be useful for this issue. What is that structure?? Yes, HFA has dissolution rate, and might work like phenol.

## Slide 7: Controlling LER is a big Challenge
There are many contributing factors.
  Stochastics in exposure (shot noise), mass transport, development, formulation heterogeneity, etc.
  In CA resists, LER is one member of the performance trade off known as the Triangle of Death.
  We will return to this issue soon

## Slide 8: Can “it” be done again at 157nm???
Perhaps….but
This time it would have been really hard!!
Could have been

## Slide 9
Wavelength (nm)
157.6 193 248
248 resist 6.84 0.37
193 resist 6.86 0.47
Polystyrene* 6.20
Polynorbornene* 6.10
PMMA* 5.69
Fluorocarbon* 0.70
Absorption (m-1) of Common Polymers
* R.R.Kunz,et al., Proc. SPIE 3678, 13 (1999).
Transmission
0.00001%!!!
Vacuum UV
O2, H2O absorbs at this wavelength
Even hydrocarbons like butane and polyethylene absorb strongly

## Slide 10
(2.68 m-1)
(2.44 m-1)
(1.15 m-1)
Absorbance of Fluorinated Polymers
Hexafluoroisopropyl and a-trifluoromethylcarboxylic acid
are groups surprisingly transparent!
(6.02 m-1)
(5.42 m-1)

## Slide 11
Images in UT 157nm Resists
70nm
85nm
90nm
60nm
Issues include: Pace, Resist, Pellicles, CaF2, Birefringence, Cost, etc.
Intel Announcement

## Slide 12
EUV Resist Progress
30mJ/cm2
MET@LBNL
18nm LS
17nm LS
16nm LS
15nm LS
Ultimate resolution of EUV resists has been improved by optimization of resist materials, illumination optics and phase shift mask.

## Slide 14: The Dose – resolution Trade off

## Slide 15
EUV Resist Resolution
Ref: H. Solak, Paul Scheerer Institute – MNE 2005, Vienna,
EUVIL Test Results with PMMA
21.25 nm

## Slide 16: The Triangle of Death
Resolution / blur
Line Edge Roughness
Sensitivity
Resolution / blur
Line Edge Roughness
Sensitivity
The area of the triangle is “constant” for a given system

## Slide 17: Can we Achieve Gain without Blur???
The catalyst is the culprit here…..
  Catalyst must move (diffuse) to achieve gain
  Movement (diffusion) causes bias and blur
  We can not escape this dilemma
Catalyst traps us in the Triangle…
  we must find a non-catalytic system with gain to escape

## Slide 18: An approach to breaking out of the triangle
Based in unzipping polymers

## Slide 19: Can we Achieve Gain without Blur???
The catalyst is the culprit here…..
  Catalyst must move (diffuse) to achieve gain
  Movement (diffusion) causes bias and blur
  We can not escape this dilemma
Catalyst traps us in the Triangle…
  we must find a non-catalytic system with gain to escape

## Slide 20: Can Escape from the Triangle of Death?
We are exploring systems that achieve gain through exploiting “unzipping” polymers
  Design provides many chemical reactions/photon..Gain
  The reactions do not involve a catalyst
  Reactions are limited to a single polymer chain
    No interchain transfer of reactivity…. No diffusion blur!!

## Slide 21
b
Requirements
Efficient unzipping in thin glassy films
Inherently sensitive to radiation
Thermally stable
Phase compatible with matrix polymer

## Slide 22: “Unzipping” polymers

## Slide 23: Aromatizing Polymer
Monomer synthesis
Notes: Carbodiimidazole—carbonyl imidazole

## Slide 24: Polymer Synthesis

## Slide 25: cis-Isomer gives a cyclic tetramer
Cyclic tetramer nmr
Molecular Formula: C32H32O8
Exact Mass: 544.21
+ 23 = 567.2
X-ray

## Slide 26: UV Exposure Study Surprise!!
Unexposed
12 h dark
1.5 h exposure
Solution quantum Yield (Φ) = 0.85 ± 0.04

## Slide 27
Novolac/Diazoquinone Photoresists
Develop
Inhibited Novolac (I)
LogR
Novolac
UV
Coat
Expose
Substrate
I
I
I
I
I
I
I
I
I
I
I
I
Substrate
I
I
I
I
I
I
I
I
P
P
P
P
P
P
Substrate
I
I
I
I
I
I
I
I
UV
Photoproduct (P)
365-nm exposure
Add DNQ
I
P
Notes: The first example -- Diazonaphthoquinone/Novolac chemistry.
These photoresists operate by taking the base soluble polymer, novolac and adding a small amount of a photoactive dissolution inhibitor, diazonaphthoquinone.
Adding the DNQ causes the dissolution rate of the resist to decrease by several orders of magnitude.
The DNQ acts as the photochemically solubility switch, such that upon exposure to 365 nm light, it’s converted to a carboxylic acid.
And this exposed resist has a higher dissolution rate than the novolac alone.
The result of this change in dissolution rate is a resist image with a nearly vertical sidewall profile.
Looking at this, you’d think that the perfect resist already exists .. And it does ... Unless you want to decrease the size of the image.

## Slide 28
Gain without a catalyst
Develop
Resin Inhibitor
(I)
LogR
Resin
UV
Coat
Expose
Substrate
I
I
I
I
I
I
I
I
I
I
I
I
Substrate
I
I
I
I
I
I
I
I
P
P
P
P
P
P
Substrate
I
I
I
I
I
I
I
I
hn
Photoproduct
(P)
exposure
Add polymer
I
P
“unzip” Polymer
Monomer
Notes: The first example -- Diazonaphthoquinone/Novolac chemistry.
These photoresists operate by taking the base soluble polymer, novolac and adding a small amount of a photoactive dissolution inhibitor, diazonaphthoquinone.
Adding the DNQ causes the dissolution rate of the resist to decrease by several orders of magnitude.
The DNQ acts as the photochemically solubility switch, such that upon exposure to 365 nm light, it’s converted to a carboxylic acid.
And this exposed resist has a higher dissolution rate than the novolac alone.
The result of this change in dissolution rate is a resist image with a nearly vertical sidewall profile.
Looking at this, you’d think that the perfect resist already exists .. And it does ... Unless you want to decrease the size of the image.

## Slide 29: Dissolution Inhibition of m-cresol Novolac
Novolac
Unzip polymer

## Slide 30: Etch performance for resist candidates
Novolak/Unzip formulation etches at a rate comparable to i-line resist.
PNBHFA/Unzip formulation etches at a rate similar to PMMA (193 nm) resist.
CF4/CHF3 etch chemistry

## Slide 31
Chart: Dose (μC/cm2)
| 0 | 60 | 80 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240 | 260 | 280 | 300 | 320 | 340 | 360
PMMA | 100 | 98.5166 | 97.751 | 96.3516 | 94.4082 | 92.0207 | 86.5758 | 82.7349 | 76.2079 | 67.4717 | 57.8361 | 41.9857 | 25.8301 | 8.8458 | 6.1278 | 4.0717 | -3.0098
Aromatizing polyester | 100 | 96.8428 | 96.6287 | 93.2343 | 87.4479 | 78.7821 | 64.7584 | 55.1865 | 41.823 | 28.6034 | 19.0031 | 5.0268 | -1.8836 | -2.8789 | -1.6448 | -1.2206
Dose to clear
= 300 μC/cm2
Dose to clear
= 85 μC/cm2
+
60 μC/cm2
50
40
30
20
10
0
Contrast Curve Study

## Slide 32: Sensitivity to electron beam radiation
100 nm line/space patterns made using Novolac/Unzip blend

## Slide 33: Mn of unzip polymer affects resist performance
Chart: Dose (μC/cm2)
| 40 | 50 | 60 | 70 | 80 | 85 | 90 | 95 | 100 | 110 | 120
2.5 kDa | 0.94 | 0.9 | 0.86 | 0.73 | 0.63 | 0.57 | 0.46 | 0.39 | 0.34 | 0.09 | -0.02
Novolak/unzipping polymer | 0.94188 | 0.91955 | 0.89265 | 0.85762 | 0.82095 | 0.76321 | 0.70318 | 0.55728 | 0.49546 | 0.36965 | 0.23437 | 0.11613 | 0.067992 | 0.06444 | 0.040024
Mnunzip = 2.5 kDa
γ = 2
D0 = 115 μC/cm2
Mnunzip = 7.0 kDa
γ = 1.95
D0 = 85 μC/cm2
PAB: 95°C, 1 min
Developer: 2.38% TMAH, 1 min
100 nm line/space patterns
Scale bar = 100 nm

## Slide 34: A resin other than novolac?
15% unzip/85% Novolak, PAB = 95C
15% unzip/85% PNBHFA, PAB = 95C
Poly(norbornene hexafluoroalcohol)
Novolak
Scale bar = 100 nm
30 μC/cm2
120 μC/cm2

## Slide 35
PMMA 450 mC/cm2
Unzip 30 mC/cm2
Acid Catalyst 145 mC/cm2
100 KeV exposure or 100 nm Lines and spaces at UMN

## Slide 36
PMMA
Ocular LER Analysis
Unzip Resist

## Slide 37: Have we escaped from the Triangle of Death??
Are we out??
Well…..Maybe……

## Slide 38: E-beam Contrast Curve 100 KeV
Chart: Dose (uC/cm2)
| 10 | 13 | 16 | 19 | 22 | 25 | 28 | 31 | 34 | 37 | 40 | 43 | 52
E-beam Contrast Curve for PNBHFA/unzip | 0.82597 | 0.73307 | 0.65859 | 0.60024 | 0.51864 | 0.38833 | 0.31432 | 0.18568 | 0.087808 | 0.056115 | 0.047353 | 0.025541 | 0.00055928
Dose-to-clear 36 uC/cm2

## Slide 39: EUV Contrast Curve (with Intel at LBL)
Chart: Dose (mJ/cm2)
| 0.19999999999999785 | 0.39999999999999786 | 0.59999999999999787 | 0.79999999999999782 | 0.99999999999999778 | 1.1999999999999977 | 1.3999999999999977 | 1.5999999999999976 | 1.7999999999999976 | 1.9999999999999976 | 2.1999999999999975 | 2.3999999999999977 | 2.5999999999999979 | 2.799999999999998 | 2.9999999999999982 | 3.1999999999999984 | 3.3999999999999986 | 3.5999999999999988 | 3.7999999999999989 | 3.9999999999999991 | 4.1999999999999993 | 4.3999999999999995 | 4.5999999999999996 | 4.8 | 5 | 5.2 | 5.4 | 5.6000000000000005 | 5.8000000000000007 | 6.0000000000000009 | 6.2000000000000011 | 6.4000000000000012 | 6.6000000000000014 | 6.8000000000000016 | 7.0000000000000018 | 7.200000000000002 | 7.4000000000000021 | 7.6000000000000023 | 7.8000000000000025 | 8.0000000000000018 | 8.2000000000000011 | 8.4 | 8.6 | 8.7999999999999989 | 8.9999999999999982 | 9.1999999999999975 | 9.3999999999999968 | 9.5999999999999961 | 9.7999999999999954 | 9.9999999999999947
UTUz18-7-3DCT 02A | 0.87501 | 0.77255 | 0.66284 | 0.35904 | 0.23362 | 0.16658 | 0.13008 | 0.097152 | 0.077223 | 0.052529 | 0.034333 | 0.024369 | 0.015705 | 0.011372 | 0.0077981 | 0.004224 | 0.0027077 | 0.0015163 | 0.00075815 | -0.00010831 | -0.00086646 | -0.00032492 | -0.00075815 | -0.00086646 | -0.0012997 | -0.00086646 | -0.0017329 | -0.001408 | -0.00086646 | -0.0027077 | -0.0025994 | -0.0025994 | -0.0030326 | -0.0031409 | -0.0034658 | -0.0027077 | -0.0035741 | -0.0035741 | -0.0032492 | -0.002816 | -0.0036824 | -0.0034658 | -0.0034658 | -0.0040074 | -0.0038991 | -0.0047655 | -0.0048738 | -0.0050904 | -0.0050904 | -0.0053071
Dose-to-clear 1.6 mJ/cm2
Notes: Megaposit MF-26A (w/ polyglycol)
Microposit MF -CD-26

## Slide 40: Resist and Process Development
Basic
Chemistry
Formulation and Process Development
Optimization
Performance
Time

## Slide 41
b
Performance Optimization Takes Time

## Slide 42: 193 nm Resist Evolution
Version 2
COMA
COBRA
150
140
130
nm
140
130
120
nm
140
130
120
nm
170
160
145
nm
160
150
140
nm
AZ®AX™1020P
AZ®AX™1000P
170
160
nm
