## Slide 1: Lecture 24
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Final Exam
When: Thursday December 13th from 9:00 am – Noon
Where: ETC 2.114
Bring Pencil, eraser....no calculator.
Corrected Exams will be available for you in NHB 5.136 after the grades are posted.

## Slide 3
Exposure Systems
“Steppers and Scanners”
R= k
l
NA

## Slide 4: Optical Lithography Limits
n = 1.44 (Water)
k1 = 0.3
l = 193 nm
sinq = 0.9
R = 45 nm
R = minimum feature size, l = wavelength
n = refractive index, θ = capture angle of lens

## Slide 5: Only option is double exposure?
=
+
20nm lines and spaces

## Slide 6
SADP
$ ₩ ¥ € !
can it be cheaper?

## Slide 7: Breaking Rayleigh's Rule

## Slide 8: How to achieve pitch division
Aerial Image
Mask
E0
Resist
Profile
Conventional Resist System
The frequency on the wafer plane is SAME as that on the mask.
Aerial Image
Mask
E0
P
Resist
Profile
Pitch Division Approach
En
N
One space on the mask prints TWO spaces on the wafer plane.

## Slide 9
Chart: 
Dissolution Threshold Dose
Insoluble
Soluble
Eo
Threshold like Response of ArF Resist
Eo

## Slide 10: Dual-tone resist
Insoluble
Insoluble
Dissolution Threshold, Eo
Dissolution Threshold, En
Soluble
Chart: Position (x)
P
N
P
N
P
N
P

## Slide 11: How do we introduce another threshold?
Adapted from 2018 Prelim Talk_Ji Yeon Kim
Dose
Dose
[Acid]
E0
Film Thickness
Dose
Film Thickness
Conventional Resist
Threshold Acid
Concentration
Insoluble
Soluble
Dose
[Acid]
E0
En
Film Thickness
Pitch Division Resist
Add Base!!

## Slide 12: Photoactive System And Mechanism
Net Acid
Acid
ka
Base
kb
hv
hv
Salt (Inert)
PAG
Photobase generator (PBG)
[PBG]0 > [PAG]0
kb < ka
Notes: So how do we achieve the near-parabolic acid profile? Use base!

## Slide 13: Photobase Generator (PBG)
Suyama et al., Progress in Polymer Science, 34 (2009) 194-209.
Houlihan et al., Macromolecules, 21 (1988) 2001-2006.
Cameron et al., J. Am. Chem. Soc., 113 (1991) 4303-4313.
DIPA-CARB
Notes: Nitrobenzyl group?

## Slide 14: A Test Formulation
MAdMA:GBLMA (50/50)
Photobase generator
(PBG)
Photoacid generator (PAG)
CONDITIONS:
6.5 wt% of PAG to polymer
PBG/PAG molar ratio = 3
PEB: 121.5 ºC, 60 sec
BARC (89 nm)
E0
En
f

## Slide 15: Lithography Result
DCHA-CARB
220 nm pitch
NA = 0.22, 440 nm pitch aerial image
220 nm pitch
k1 = 0.15!!!
Notes: Rough LER every alternate line

## Slide 16: Low chemical contrast

## Slide 17: Increasing Chemical Contrast (Acid Gradient)
With Nick Turro from Columbia
Conventional PBG
2-Stage PBG
2-Stage PBG improves chemical contrast!!

## Slide 19
Photo-aromatization type 2-stage PBGs
Norrish II
Step 1
Step 2
keto
Enol
Latent PBG
PBG
hn
base
base

## Slide 20: Contrast curve under 193nm
Chart: 
| 3.14 | 6.28 | 9.42 | 18.84 | 21.98 | 25.12 | 28.26 | 31.4 | 34.54 | 37.68 | 40.82 | 43.96 | 47.1 | 50.24 | 56.52 | 62.8 | 69.08 | 75.36 | 87.92 | 100.48 | 125.6
 | 0.91673 | 0.90953 | 0.89227 | 0.9047 | 0.88643 | 0.91634 | 0.56772 | 0.053738 | 0.021749 | 0.019654 | 0.022081 | 0.034383 | 0.032555 | 0.049791 | 0 | 0.024637 | 0 | 0.026368 | 0.79932 | 0.88993 | 0.90165
mJ / cm2
Normalized Thickness remaining

## Slide 24: More Recent Results
Chart: Exp Time (min)
| 0 | 1 | 2 | 3 | 5 | 10 | 20 | 30 | 40
Aniline | 0 | 0.026941 | 0.080911 | 0.11686 | 0.36236 | 0.99873 | 1.722 | 2.1822 | 2.4427
1 Stage | 0 | 0.23009 | 0.41968 | 0.55577 | 0.89451 | 1.0945 | 0.84721 | 0.56825 | 0.40624
2 Stage | 3.1655 | 2.9982 | 2.8087 | 2.6257 | 2.1794 | 1.4763 | 0.55995 | 0.24518 | 0.12108
Nonlinear!!
Chart: 
| 0 | 1 | 2 | 3 | 5 | 10 | 20 | 30 | 40
Aniline | 0 | 0.026941 | 0.080911 | 0.11686 | 0.36236 | 0.99873 | 1.722 | 2.1822 | 2.4427
1 Stage | 0 | 0.23009 | 0.41968 | 0.55577 | 0.89451 | 1.0945 | 0.84721 | 0.56825 | 0.40624
2 Stage | 3.1655 | 2.9982 | 2.8087 | 2.6257 | 2.1794 | 1.4763 | 0.55995 | 0.24518 | 0.12108

## Slide 25: Demonstration with IBM
2-Stage Cross Section
1-Stage Cross Section
CHA-NO2
CHA-bisNO2
Notes: Solve the LER issue

## Slide 26: Demonstration with IBM
193
Notes: Much improved LER

## Slide 27: Will this work???
Great students are working hard
Time will tell!!
Dr. Xinyu Gu

## Slide 28: Ryan Mesch

## Slide 29: Shifting to longer wavelength (365 nm l)
https://www.mysmarttvs.co.uk/products/samsung-ue55ks9000-smart-4k-ultra-hd-hdr-55-curved-led-tv
Image from Canon,
Oh no…I don’t want to buy this again
I-line Flat Panel Lithography Tool

## Slide 30: Pitch division at i-line (365 nm l)
Negative Tone Resist
Positive Tone Resist
Early proof of concept by Paul Meyer and Cameron Adams
Early proof of concept by
Ji Yeon Kim

## Slide 31: The I-liners
Paul Meyer
Ji Yeon Kim
Patrick Harold
Daniel Bonnecaze
Cameron Adams

## Slide 32: Thank you!!