## Slide 1: Lecture 3
Chemical Engineering for Micro/Nano Fabrication

## Slide 2
ILLUMINATION
MASK
WAFER
RESIST
Modulation of the mask is ?
Modulation of the image is ?
Modulation in Contact Printing
1
~1
The image is almost perfect!
Imax – Imin
Imax + Imin
MODULATION =
Notes: Problem is that the mechanical contact between the mask and wafer causes defects on the mask and wafer with consequent negative impact on productivity.

## Slide 3
Some change required to go forward
As dimensions decrease, so do yields!
Serious Problems with Mask Contamination
  Rubber resist and Emulsion Masks
  Introduction of Chromium on glass masks
Alignment was done external to the Exposure system
  Slow production and low yield = 
Just move the mask away and do…
  “Proximity Printing”

## Slide 4
But…..Nothing is Simple

## Slide 5
Newton vs Fresnel
Diffraction rears it’s head
Nothing is Simple…it seems
Notes: Hence the introduction of proximity printing. However, the resolution degrades significantly at practical mask gaps.
Typical separation in proximity printing is 20 – 50 um

## Slide 6
Huygens’ Theory
When w = l 1 wavelet
Many wavelets that interact
Wavelets

## Slide 7
Image can be constructed from point sources of spherical wavelets in the opening (Huygens’ Theory)
There is interference between these waves that causes “ringing”
Here the minimum feature size is W ~ lg
For g = 20 mm and 365 nm light, W is on the order of 2.7 mm
Fresnel Diffraction in Proximity Printing
Near field or Fresnel Diffraction Regime When g < W2/l

## Slide 8
We also have have Frauenhofer Diffraction
Far Field Diffraction.

## Slide 9
Brief Look at Diffraction
Some Excellent Video Lessons
https://www.youtube.com/watch?v=blur0MemUQA
1. Constructive and destructive Interference
https://www.youtube.com/watch?v=7CmbItRjM-Y
2. Single Slit Diffraction
https://www.youtube.com/watch?v=Pk6s2OlKzKQ
6. Double slit Diffraction – Part 1
https://www.youtube.com/watch?v=1abpdO27KTo
7. Double Slit Diffraction - Part 2
https://www.youtube.com/watch?v=Iuv6hY6zsd0
3. Double slit waves 2:00
https://www.youtube.com/watch?v=nuaHY5lj2AA
5. Double Slit Demonstration
https://www.youtube.com/watch?v=PgW7qaOZD0U
4. Single slit diffraction demonstration

## Slide 10
…When the width is small the gap must be small
So ….. we can do projection printing
  and get the mask far away from the wafer

## Slide 11: Optical Aligner Design Principles

## Slide 12: Advantages of Projection Printing
Non-contact operation which prevents the mask from introducing defects and wearing out.
No need for replacement masks.
Wafer images are potentially more uniform because a single “mask” is used for all of them.
Improved alignment accuracy – no need to move the wafer after alignment.
Reduction capability makes masks easier to fabricate and repair.
Mask can be protected with a pellicle

## Slide 13: The Pellicle