## Slide 1
Lecture 5
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: For a Rigorous modeling of Proximity Printing limits see:
Simulation of proximity printing
W. Henke, M. Weiss, R. Schwalm and J. Pelka Microelectronic Engineering 10 (1990) 127-152
Crude relationship between wavelength (l), gap (g) and the minimum width of a feature
where k = 1-2

## Slide 3
Image can be constructed from point sources of spherical wavelets in the opening (Huygens’ Theory)
There is interference between these waves that causes “ringing”
Here the minimum feature size is W ~ lg
For g = 20 mm and 365 nm light, W is on the order of 2.7 mm
Fresnel Diffraction in Proximity Printing
Near field or Fresnel Diffraction Regime When g < W2/l
From Lecture 3

## Slide 4
We also have have Frauenhofer Diffraction
Far Field Diffraction.
Please look carefully at these inequalities. Are they correct?
From Lecture 3

## Slide 5
Feature size is directly related to the
wavelength of the exposure radiation
Resolution Limit of the Projection Printing
Theoretical Resolution
F= k1
l
NA
F :
l :
k1 :
NA :
n :
Minimum feature size
Exposure wavelength
Process-dependent factor
Numerical aperture of lens system
Index of refraction (for air, n  1)
Aperture
Entrance
Pupil
qmax
NA = n sin qmax

## Slide 6: Wave Length Reduction History

## Slide 7
Lithographic Lens Evolution
Starlith 500 Lens (Zeiss)
Notes: The PAS 5500/850 248nm DUV step and Scan
Starlith 500 Lens from Carl Zeiss – used in ASML PAS 5500/550B scanner for 180nm processes and a 26x33mm field.

## Slide 8
The stepper lens has a numerical aperture of NA = 1.35(huge!) and is intended for use in immersion lithography, a technique that replaces the air gap between wafer and stepper with water or another fluid. Zeiss notes that the device is, in some sense, the end of the art. The lens is designed for an UV light source with a wave length of 193 nm, which needs an ArF (yes, "Argon Fluoride") Laser. Remember that the visible spectrum ends around 400 nm. UV radiation from the sun, for comparison, spans the range (315 - 400) nm ("Ultraviolet A") and (280 - 315) nm ("Ultraviolet B").
The producer of this lens is Carl Zeiss SMT AG , Germany.
193 nm Immersion Lens

## Slide 9
State of the art, 193 nm exposure tool
l = 193nm
NA = 1.35
K = 0.3
Catadioptic Lens design

## Slide 10
Focusing Light

## Slide 11: Snell’s Law

## Slide 12
https://www.youtube.com/watch?v=37H5jJmHh2Y
Off Axis Imaging
Imaging more than one spot or slit

## Slide 13
Aperture
Entrance Pupil
qmax
NA = n sin qmax
0
+1
-1

## Slide 14
Aerial Image of a 56 nm grating

## Slide 15: Aerial Image for the Aligner Designs

## Slide 16: Chemist’s view of how things really work
aerial image
$$$$$$$$$$$$$
Amazing Chemistry!!
resist image
aerial image
Mask
aerial image
at the wafer
¢¢¢¢¢¢!!!

## Slide 17: Non-linear dissolution rate response

## Slide 18: Threshold like Response of ArF Resist
E0

## Slide 19
Oil Immersion Microscopy

## Slide 20
Liquid Immersion Lithography
Source: Nikon
Notes: Only the final optical element and its housing, the wafer and stage are in contact with the immersion fluid.
High through-put Step and Scan Lithography where the wafer moves through exposure could be problematic because of fluid turbulence and index non-uniformities.
Small changes in temperature within the fluid would cause relatively large changes in focus position. Depending on dn/dT which would be difficult to control at high throughput.
Finally, imaging layer would have to be extremely thin.
All ducks are in a row for device manufacturing around 2007.
Technology is expected to work at both the 65nm and 45nm process nodes.
Availability of HyperNA lenses with NA >1.

## Slide 21
Immersion Microscopy
Fluid Here!
More orders are captured!!!

## Slide 22
Fluid is here!?
Mask
Wafer
Immersion Lithography
No new rays are captured!!!

## Slide 23: Chemist’s View of Immersion
Adding water to the space between the final lens and the wafer does not improve resolution.
It does improve depth of focus and therefore process latitude
It does allow design of high NA lenses that would otherwise not work!
Immersion Lens

## Slide 24: Critical angle & total internal reflection
https://en.wikipedia.org/wiki/Total_internal_reflection

## Slide 25
Notes: Note: The addition of water to existing lenses does not increase the numerical aperture. Lenses of a given NA designed to operate in air can be modified to function as immersion lenses but their NA will typically be unchanged.

## Slide 26
SPIE 2003 Feb.28 Santa Clara ML5048
-
68 Ohmura et. al.
Slide 1
0.6
0.7
0.8
0.9
1.0
1.1
1.2
Lens diameter vs. NA
Lens diameter vs. NA
NA
Lens Diameter (A.U.)
All Spherical
Liquid Immersion
With
Aspheres
（4X, 26x33mm field)
$$$$$$$$$$$$$$$$

## Slide 27: A Prophetic Advertisement??
Size Matters????

## Slide 28: Optical Lithography Limits
n = 1.44 (Water)
n = 1 (Air)
k1 = 0.3
l = 193 nm
sinq = 0.9
R = 65
k1 = 0.3
l = 193 nm
sinq = 0.9
R = 45
≠ 22 !!

## Slide 31
Limitations of water
Indices of refraction for water immersion.
  SiO2: 1.56
  CaF2: 1.51
  Water: 1.435
  Resists ~ 1.70
0.93*1.435 = 1.33
nsinθ ≤ 0.93* min(nglass, nfluid, nresist)
If k=0.25, R = 36nm

## Slide 32
Options beyond water
Options for high index immersion lithography.
  Glass.
    BaLiF3: 1.64
    (Lu3Al5O12, LuAG): 2.1
    (Mg3Al2Si3O12,Pyrope): 2.0
  Fluid.
    Cyclic organics, such as decalin: 1.64-1.65

## Slide 33: High Index Materials
Fluid
n = 1.64
Decalin
R= 37nm
No candidate has been identified for high index fluid or high index resist.
2nd generation
LuAG (n = 2.1)
n = 1.9*
Lens
Fluid
Resist
n = 1.8
3rd generation
R= 32nm

## Slide 34: Cyclohexane
99+% Purity
1 – Sulfuric Acid Wash
2 – Sulfuric Acid Wash, Silica Gel Chromatography
3 – Sulfuric Acid Wash, Silica Gel Chromatography, Distillation
Wavelength (nm)
Absorbance (cm-1)
4 – Sulfuric Acid Wash, Silica Gel Chromatography, Distillation, De-oxygenation

## Slide 35: Absorbance Edge

## Slide 36: Cycloalkanes
Density 1.07 g/cm3
x
n193 = 1.73
Abs193 = 0.13
Highest RI is expected
López-Gejo et. al., Chem. Mater.19, 3641-3647 (2007)

## Slide 38: What variable is left to be optimized?
We have discussed l
  I told you that 193nm is the lower limit
We have discussed NA
  I told you that 1.35 was the upper limit
The only thing left is…..
“k”
R= k
l
NA

## Slide 39: Rayleigh’s Rule…”k”
The Nobel Prize in Physics 1904
1842-1919
John William Strutt, third Baron Rayleigh

## Slide 40: Sir George Airy
Airy disk is a description of the best focused spot of light that a perfect lens with a circular aperture can make
F

## Slide 41
Lord Rayleigh defined this criterion: when the first minimum of one Airy disk coincides with the maximum of another ->
Rayleigh’s Rule for Resolution

## Slide 42
When a single point of light is imaged it becomes the point spread function (PSF) of the lens system.
  For an ideal, circular imaging system, the PSF is called the Airy disk:
  The FWHM of the Airy disk is 0.5 l/NA, which defines the smallest image of a point source
Defining the resolution of an imaging system