## Slide 1
Lecture 6
Chemical Engineering for Micro/Nano Fabrication
Let there be light

## Slide 2: Rayleigh’s Rule…”k”
The Nobel Prize in Physics 1904
1842-1919
John William Strutt, third Baron Rayleigh

## Slide 3
Lord Rayleigh defined this criterion: when the first minimum of one Airy disk coincides with the maximum of another ->
Rayleigh’s Rule for Resolution

## Slide 4
When a single point of light is imaged it becomes the point spread function (PSF) of the lens system.
  For an ideal, circular imaging system, the PSF is called the Airy disk:
  The FWHM of the Airy disk is 0.5 l/NA, which defines the smallest image of a point source
Defining the resolution of an imaging system

## Slide 5
sin max  NA = /pmin
sin max  2NA = /pmin
Normal Incidence
Oblique Incidence
+1
-1
-1
0th
0th
Mask
Objective
Lens
Lithography breaks Rayleigh’s rule

## Slide 6: We need a Next Generation Lithography The “NGL”s

## Slide 7: Next Generation Lithography - NGL
SEMATECH and the ITRS
  Beyond the 22 nm node
Optical Lithography | Electron Beam Litho.
High throughput Resolution limited EUV? | High Resolution Serial process Cross over Problem

## Slide 8: X-ray Proximity Printing

## Slide 9: LIGA Process
LIGA is the german acronym for lithography, electroplating and moulding (Lithographie, Galvanik und Abformung).

## Slide 10: The LIGA Process and MEMS Micro Electo Mechanical Systems

## Slide 11: LIGA PROCESS

## Slide 12: 3 Axis Accelerometer EE-UC Berkeley

## Slide 15
RUN OUT ERROR
Run out mag error
d = rg / L
Penumbral blur
δ = ag / L
Source needs to be very far away!
but intensity proportional to 1/L2

## Slide 22: In the end….
Over lay and mask issues killed the x-ray program
  Distortion due to patterning
  Heating
  Optical transparency issues
Optics caught up and was cheaper, faster and safer.
  I-line steppers could out perform the x-ray system
LIGA led to MEMS which is alive and well

## Slide 23: The Landscape is littered with NGL’s
Electron Beam direct write
Write with many electron beams
Project electron beams
157nm Photolithography
Shadow printing with Synchrotron X-rays
157nm
X-ray
157nm
X-ray

## Slide 24: Focused ion beam lithography

## Slide 25: Liquid Metal Ion Source

## Slide 26: Inelastic (Electronic) Collisions
Conversion of KE to other forms of energy
  Required for ion induced chemical reaction
Negligible scattering of incident ion
Ionization of target atoms and SE generation
  SE play significant role in bond dissociation – resists
[6]

## Slide 27: Motivation: Ions
Small particle wavelength -Not diffraction limited
Large Mass
  Less scatter – No proximity effects
  Delivery more energy than e-
Additional capabilities:
[2]

## Slide 28: Physical Milling or Sputtering
Ability for resistless structuring
Elastic Cascade Model
Sputter or Milling Yield
  Target atom
  Ion species and energy
  Angle of incidence
  Orientation dependent
Slow – high dose req.

## Slide 29: Gas Assisted Etching (GAE) and Deposition (GAD)

## Slide 30: Resists for IBL
Secondary electron induced bond dissociation
Energy deposition dependent resist
  Low mass to energy ratio – electric stopping
  High mass to energy ratio – nuclear stopping
Positive tone resist becomes negative
  Crosslinking induced by radicals liberated by ions
  Pattern both pos./neg. by varying energy!

## Slide 31: Ion Beam Properties
Energy spread leads to chromatic aberration (blur)
Space charge effects add to energy spread
Beam diameter proportional to beam energy
Ga+
Ga+

## Slide 32: Ion Projection Lithography: Masks
Thin metal membrane (Si) with apertures
Control issues:
  Stress relief & thermal expansion
Overlay or “Donut Problem”
Target
Feature
A Mask
B Mask

## Slide 33: Future Outlook
Multibeam tool: 43-APS by IMS
  Gas discharge broad beam
  Programmable shutter aperture plate
  43,000 beams, demagnification 200x
  Ion dot matrix printing for NIL*
[2]

## Slide 34
X-ray Mirrors Created at LLNL and Sandia
Film Stack
Reflectivity
Fortunately, …..on the Horizon is….EUV

## Slide 35
A “Phase Defect

## Slide 36: EUV Mirror

## Slide 37
The path to success is 11nm EUV??

## Slide 39: Large, complex, costly solution
0.69  0.00  P(success) !!

## Slide 40
EUV Mask
Ultem Substrate
Ruthenium
Tantalum boron nitride
Chromium Nitride
Silicon Dioxide
Molybdenum Silicon Stack

## Slide 41
Living with Defects

## Slide 42
EUVL
Let there be light!

## Slide 45: This is just an EUV light bulb that is 100x to dim!!
Large, complex, costly solution

## Slide 46: Cymer EUV Light Source

## Slide 47
What is under the floor – out of sight

## Slide 48
A Laser Bank

## Slide 49
Source produces “out of band” radiation as well as EUV