## Slide 1
Lecture 7
Chemical Engineering for Micro/Nano Fabrication

## Slide 2: Optical Lithography Limits
n = 1.44 (Water)
k1 = 0.3
l = 193 nm
sinq = 0.9
R = 45
R = minimum feature size, l = wavelength n = refractive index, θ = capture angle of lens

## Slide 3: The Landscape is littered with NGL’s
Electron Beam direct write
Write with many electron beams
Project electron beams
157nm Photolithography
Shadow printing with Synchrotron X-rays
157nm
X-ray
157nm
X-ray

## Slide 4
Is this the end…of Moore’s Law??
This cannot be!!!
It would lead to economic collapse

## Slide 6
MITI
Applying enough money and brains has always solved our problems
SEMATECH
DARPA
Artist: Bruce Marion
Can’t bridge the gap!!!?? 
Intel Plows $4.1 billion Into Next-Gen Chip Production
TSMC eyes future technology with $1.4 billion …. Investment

## Slide 7
Extreme ultraviolet lithography:
overview and development status
Peter J. Silverman
Intel Corporation
Santa Clara, California 95054
J. Microlith., Microfab., Microsyst. 4(1), 011006 (Jan–Mar 2005)

## Slide 8
EUVL “Critical Issues”

## Slide 10
HOPE

## Slide 12
Gap?

## Slide 13: 2017 EUV Brightness data
Proc. of SPIE Vol. 10143 1014306-1

## Slide 14
Absorbance now between 10 and 20%

## Slide 16
1995 Predictions by Gordon Moore

## Slide 17
1995 Predictions by Gordon Moore

## Slide 18
Exposure Tool Price versus Time
Various Manufacturers
$100,000
$1,000,000
$10,000,000
$100,000,000
1975
1980
1985
1990
1995
2000
2005
2010
Tool Price ($)
Includes historical data for both steppers and scanners of all
makes and models from various manufacturers including
ASET, ASML, Cameca Instruments, Censor AG, Canon, Eaton,
GCA, General Signal, Hitachi, Nikon, Perkin-Elmer, SVGL,
and Ultratech.
193nm steppers
157nm ?
 E U V ?
Last Published cost was 2010 …$120M

## Slide 19
EUV tool costs hit $120 million
Mark LaPedus
11/19/2010 6:55 PM EST
SAN JOSE, Calif. - Who can afford extreme ultraviolet (EUV) lithography? Answer: Very few companies. And the tool price tag is going up. ''EUVL: and the price is? The answer is...$125 million'' per tool, said G. Dan Hutcheson, CEO of VLSI Research Inc., in a report. ''Don’t choke. Years ago, (Risto Puhakka, president of VLSI Research) predicted this with a cost-per-pixel analysis. Everyone thought he was insane at the time…

## Slide 20
Exposure Tool Price versus Time
$1,000,000
$10,000,000
$100,000,000
1990
1995
2000
2005
2010
Tool Price ($)
$200,000,000
2017

## Slide 21
EUV uses ca 13,000 KwH/day
Requires > 500,000 gallons of cooling H20 / day
1 KwH represent, for example, the power required to operate a 100 w light bulb for 10 Hours.
A typical house consumes ca 850 KwH / MONTH
There are several assessments of COO for EUV available in the literature….caution…carefully review the assumptions
If you consider depreciation of the capital cost…the COO numbers are VERY high.
High Cost of Ownership

## Slide 22: Rising Cost of Wafer Fabs Vs. GNPs
0.01
0.1
1
10
100
1000
0.01
0.1
1
10
billion $
feature size [µm]
Luxemburg
Panama
Singapore
Hungary
Czech Rep.
Kenya
Denmark
Monaco
GNP of:
Guatemala
100 nm
technology
node, 2004
70 nm
technology
node, 2007
35 nm
technology
node, 2013
Macedonia
50 nm
technology
node, 2010
?

Ralph Dammel SPIE 2002

## Slide 24
Lithography expert Christopher Mack wrote about ASML’s EUV presentation at the 34th International Conference of Photopolymer Science and Technology in early July. When asked when its equipment would be ready for manufacturing insertion, ASML claimed second half of 2018. Mack writes:
I laughed out loud when I heard that. When I asked if that prediction was serious, the response was “it depends on how you define manufacturing.”

## Slide 25
Gordon Moore, Lithography and the Future of Moore's Law [Proc. SPIE Vol. 2437, May 1995]

## Slide 26: Don’t worry EUV will work….
and if it’s not ok….. it’s not the end!
in the end

## Slide 27
Oh No..what do we do now????

## Slide 28: So…we keep “tweeking” 193 immersion
Wave Front Engineering
  SRAFS (Sub resolution assist features)
  OPC (optical Proximity Correction)
  RET (Reticle Enhancement Techniques)
  Phase Shifting masks
    Of Various Designs.
  Inverse Lithography Processes
Trying to survive until we are saved by an NGL (Next Generation Lithography)
  Ion Beam
  Imprint in various Forms
  E-Beam Lithography – Multi Beam. Projection, etc.
    MAPEL, REBL, Scalpel, Mapper, Etc.
  Etc, Etc, Etc..

## Slide 29
Wavefront Engineering: OPC
Optical and Process Correction (OPC) for Amplitude Control
Rule-Based OPC - modifies layout with sub-resolution assist features to compensate for process distortions
  Add light where needed
  Subtract light where not wanted
  Add structures to layout to control diffraction of light
Lithography equipment does not form images of these features
Scatter outside the lens NA
Employs MANY engineers
Notes: OPC applies systemmatic changes to photomask geometries to compensate for nonlinear distortions caused by optical diffraction and resist process effects. These distortions include linewidth variations dependent on pattern density, which affect device operating speed, and line end shortening which can break connections to contacts.
To compensate for line end shortening, the line is extended using a hammer head shape that produces a line much closer to the intended shape. To compensate for corner rounding, serif shapes are added to or subtracted from corners to produce more accurate angles. Determining the optimim type, size and symmentry or lack thereof is complex and depends on neighboring geometries and process parameters.

## Slide 30: Optical Proximity Correction SRAFs

## Slide 31
Impact of OPC on Physical Design
Design
Layout
Final
Layout
Mask
Wafer
Scatter Bars
Serifs

## Slide 32
Wavefront Engineering: Phase
l
Amplitude
Direction
Phase

## Slide 33
Wavefront Engineering: Levenson Phase Mask
Marc David Levenson, through the pioneering development of phase shifting masks, laid the ground-work for the industry's efforts at wavefront engineering and resolution enhancement technology.
Here he is with the Fritz Zernike Award
Marc
David
http://www.betasights.net/wordpress/?p=923

## Slide 34
Phase Shifting Principle
Conventional Mask
Phase Shifting Mask
Amplitude
at Mask
Amplitude
at Wafer
Intensity
at Wafer
Phase Shifter
d
d = 0.5/(n-1)
Notes: Shifting the phase by 180 degrees is equivalent to changing the sign of the amplitude.
The conventional binary mask only controls the magnitude of the amplitude, not its sign whereas a phase shifting mask controls both amplitude and sign. Allows for amplitudes of opposite signs on opposite sides of each narrow, opaque, mask feature.
Can use destructive interference to cancel some of the image spreading effects of diffraction.
Net result is a remarkable increase in contrast for fine dark features accompanies by a 180°phase shift – also DoF.
Exact degree depends on the degree of partial coherence For current illumination systems with  =0.5, the DoF improvement is about 2.

## Slide 35
Phase Shifting Mask
https://spie.org/publications/fg06_p78-80_phase-shift_masks

## Slide 36
Five means of patterning an isolated dark line. The mask structures are shown at the top with the resulting amplitude profiles in the middle. At the bottom are the in-focus intensity profiles (and the profiles at the end of an out-of-focus k2 =1 exposure window) [red]) plotted versus displacement units of k1. The transmission mask in (a) would print with a zero-bias width corresponding to k1 = 0.5. The chromeless phase edge in (b) and the Levenson-mask in c (phase edge is buried under an opaque line) produce dark lines with k1 = 0.25. The shifter-shield design in (d) projects a dark line of width k1 = 0.6 while the rimshifter mask in (e) produces a line with k1 = 0.8. Except for the transmission mask,in (a), each of these values is near the optimum for that mask structure.
Phase Shifting Designs
M. Levenson, Microlith. World, 1(1), 6 (1992)

## Slide 37
Laying out Levenson Masks

## Slide 38
Laying out Levenson Masks

## Slide 40
Two beams with same wavelength
Overlapping region
Interference lithography
Intensity modulation in the region of the overlapping of two or more coherent beams.
Advantages:
Simple and fast, no photomask or lenses.
Disadvantage:
Difficult to create anything other than a periodic structure.
Requirements:
High spatial and temporal coherence of the source.

## Slide 41
Interference lithography using incoherent light source
For an arbitrary position X on the wafer, the two beams have the same optical path (L1=L2), so no need of temporal coherence (spatial coherence is still needed).
p is pitch of phase grating. P is pitch of grating on wafer.
Pp/2, independent of .
(but must <p)
(n is refractive index)
Wafer
Phase grating
Direct-beam stop
x
Diffracted light

L1
L2
Notes: It is not easy for the student to understand this and next slide. Need to explain well first what is spatial and temporal coherence.

## Slide 42
Wavefront Engineering: Direction
Off-Axis Designs
  Annular
  Quadrupole
  Dipole
+
or
Eliminates on-axis zero order light - increases contrast
Notes: With off-axis, illumination, the image is formed by the interference of the first-order and zero-order beams (Two Beam imaging). Both beams are subject to phase differences in a defocus position, impacting contrast.
The phase difference is given by the radial position in the in the lens pupil.
Because of the off-axis character of the illumination, this difference will be less when compared to normal on-axis illumination.
In the limiting situation, the first-order and zero-order beams have the same radial position., hence the contrast degradation in defocus will be minimal. For  = 0, the contrast degradation will be zero.
In practical systems, the intensity distribution in the lens pupil must be radially symmetric. Deviations will result in an unwanted non telecentric system. This is the case with annular and quadrupole illumination.
Annular provides isotropic improvement in resolution. The others provide directional improvement.