## Slide 1
Lecture 9
Chemical Engineering for Micro/Nano Fabrication
157 nm

## Slide 2: 157 nm Lithography
F2 Excimer Laser output 157 nm
157 nm light
  Air, water, polyethylene…almost everything is opaque
  CaF2 is transparent but crystalline, birefringent
  There is no resist, no Mask material, no Pellicle, immersion Fluid, etc.
Requires a New Infrastructure
  Glass, purge gas. Mask…. Long lead times and EUV is coming ☺

## Slide 3
Wavelength (nm)
157.6 193 248
248 resist 6.84 0.37
193 resist 6.86 0.47
Polystyrene* 6.20
Polynorbornene* 6.10
PMMA* 5.69
Fluorocarbon* 0.70
Absorption (m-1) of Common Polymers
* R.R.Kunz,et al., Proc. SPIE 3678, 13 (1999).
Transmission
0.00001%!!!
Vacuum UV
O2, H2O absorbs at this wavelength
Even hydrocarbons like butane and polyethylene absorb strongly

## Slide 4
Opaque
Transparent
Fluorination of Norbornane Skeleton
248 nm
193 nm
157 nm
?
?
How many fluorines and where to fluorinate?

## Slide 5
Selective Fluorination of Norbornane
Geminal substitution at the two carbon bridge is the most effective fluorination pattern
-CF3 acrylates

## Slide 6
Surprising Serendipitous Discovery
A157 = 2.57 m-1
Originally for Top Surface Imaging Project
NBHFABOC and NBHFA are surprisingly transparent
A157 = 1.15 m-1
T. Chiba, et. al., J. Photopolym. Sci. Technol , 13 (2000) 657-664

## Slide 7
(2.68 m-1)
(2.44 m-1)
(1.15 m-1)
Absorbance of Fluorinated Polymers
Hexafluoroisopropyl and a-trifluoromethylcarboxylic acid
are groups surprisingly transparent!
(6.02 m-1)
(5.42 m-1)

## Slide 8: Encouraging Imaging Results at 157 nm
40nm
80nm
90nm
100nm
60nm

## Slide 9: Resist and Process Development
I-line
248nm
193nm
Basic
Chemistry
Formulation and Process Development
Optimization
Performance
Time
We are well off the base line
60nm
157 nm

## Slide 10
Images in UT 157nm Resists
70nm
85nm
90nm
60nm
Issues include: Pace, Resist, Pellicles, CaF2, Birefringence, Cost, etc.
Intel Announcement

## Slide 11: The Kiss of Death
intel drops 157-nm tools from lithography roadmap
Mark LaPedus
5/23/2003 01:40 AM EDT
SANTA CLARA, Calif. -- Intel Corp. has revised its lithography strategy for the second time in the recent months, disclosing it has dropped 157-nm tools from its roadmap and is not pursuing the scanner technology for IC production. The move is expected to impact fab-tool and material vendors developing 157-nm products for Intel.
El beso de la muerte, by an unknown sculptor.
Barcelona, Spain ca. 1930

## Slide 12: The Landscape is littered with NGL’s
Electron Beam direct write
Write with many electron beams
Project electron beams
All of the above with ions
Shadow printing with Synchrotron X-rays
157nm
X-ray
Now here lies 157nm …rest in peace!
157nm
X-ray

## Slide 13
157nm
X-ray
X-ray
Let’s look more closely in the graveyard

## Slide 14
Eigler, et al IBM Almaden
Xe on Nickel
Ultimate limit of high resolution patterning!!
1 atom
0,438 nm
Notes: There is a limit to resolution and this is it…one atom

## Slide 15: Consider Resolution vs. Throughput
10-6
10-4
10-2
100
10 2
104
106
108
1010
1012
STM- atom manipulation
AFM (single tip with Silicon as resist)
E-beam lithography
(inorganic resists)
Other Gaussian E-beam lithography (high speed resists)
Gaussian E-beam lithography
(PMMA resist)
Resolution (Angstrom)
Area Throughput (μm2/hr)
Don Tennant: Cornell University
Shaped & cell projection E-beam lithography
Imprint
Notes: This plot from Professor Tennant at Cornell shows that all high resolution printing methodologies fall on a line in a log-log plot that relates throughput to resolution. The single atom experiment is in the lower left….very slow, but high resolution. Optical lithography I in the upper right. There is one technique that does not fall on this line. That is imprint so we were inspired to explore this technology.

## Slide 16
90’s Soft Lithography
Soft Lithography
1. PDMS template with thiol
2. Imprint stamp
3. Transfer molecules
4. Pattern Transfer
Annu. Rev. Mater. Sci. 1998. 28:153–84
Younan Xia and George M. Whitesides

## Slide 17: 90’s Thermal Imprint Lithography
Science 5 April 1996:
Imprint Lithography with 10 -Nanometer Resolution
Stephen Y. Chou, * Peter R. Krauss, Preston J. Renstrom
NIL Process

## Slide 18
Pattern Density Effects
Easiest… Easy… Very Difficult!
“Residual layer”

## Slide 19
1980’s Nanoimprint for CDs
Phillips 2P process
  UV sensitive “lacquer” sandwiched between mold and thin polycarbonate substrate
  UV light shown through substrate to cure lacquer

## Slide 20: 2000 Step and Flash Imprint Lithography
S-FIL fluid dispenser
Ink jet system
Planarization layer
Substrate
Step 1: Dispense drops
Step 2: Lower template and fill pattern
Step 3: Polymerize S-FIL fluid with UV exposure
Step 4: Separate template from substrate
Template
Substrate
Substrate
Template
Step & Repeat
Substrate
Planarization layer
Planarization layer
Planarization layer
Fused silica template, coated with release layer
Template filling driven by capillary action
low imprint pressure and room temperature process
Template
Notes: So how does the technology work. Well before I go into the details of SFIL, lets talk about imprint technology in general. It had its genesis I suppose with the wax seals that the Chinese invested to authenticate documents, and the same thermoplastic process has been used in the past decade to make very high resolution lithography patterns – with Stephen Chou at Princeton leading the way. However, any thermal process is an absolute non starter in the CMOS industry since it makes accurate overlay impossible. The next alternative was to use a UV curable film spun onto the wafer, but now you have the challenge of moving a relative high viscosity material between the various patterns on the template, so Grant and SV came up with the idea of using a low viscosity monomer placed on the surface of the wafer.
This slides shows a schematic animation of the SFIL process:
Points to make – template is common with photolithography – smaller dimensions yes, but otherwise common to allow commercial supply – no membranes per previous NGL efforts
- process leaves a very thin film which can be removed in an etch descum. ie the process is compatible with etch. Thus the upstream template and the down stream etch and compatible. Just replace the litho cell.
- some application are whole wafer