## Slide 1: Double Patterning
Samuel Johnson
11/6/18

## Slide 2: Outline
Background
Introduction to SADP
Deposition
Trim mask issue
Self Aligned Quadruple Patterning
SADP Problems
Via Level Manufacturing

## Slide 3: Single Patterning
Lithography and Etch
  Lay photoresist
  Lithography
  Develop
Chris Mack Lecture 59 (CHE 323) Lithography Double Manufacturing

## Slide 4: Single Patterning Resolution Limit
  Theoretical Limit at 36nm
  Formula is for half pitch: full pitch is 80nm
https://http://www.aspdac.com/aspdac2013/archive/pdf/3C-4.pdf/

## Slide 5: Two Lithography Double Patterning
Litho-etch-Litho-Etch
Litho-freeze-Litho-Etch
Chris Mack Lecture 59 (CHE 323) Lithography Double Manufacturing

## Slide 6: Two Lithography Double Patterning
Problems
  Expensive: two lithography steps
  Overlay problem
https://semiengineering.com/fillcut-self-aligned-double-patterning/

## Slide 7: Self Aligned Double Patterning
Nakatama, K; et al. SPIE 2012

## Slide 8: Conformal Deposition
Step 3: Deposition of sidewall material
Thickness of deposited layer is crucial
Chris Mack Lecture 59 (CHE 323) Lithography Double Manufacturing

## Slide 9: Chemical Vapor Deposition (CVD)
Deposition method of choice
  Able to deposit on resist material and wafer
  High quality
  Anisotropic process
  Industrially viable
Chris Mack Lecture 59 (CHE 323) Lithography Double Manufacturing

## Slide 10: Chemical Vapor Deposition (CVD)
CVD is simple and cheap
High temperature
Meets criteria listed before

## Slide 11: Etching
Etch time and conditions will determine material etched
  Etching too long will result in different sized features
https://semiengineering.com/fillcut-self-aligned-double-patterning/

## Slide 12: Trim Mask Issue
Sidewall forms all around patterns-loops
A problem if not desired
Chris Mack Lecture 59 (CHE 323) Lithography Double Manufacturing

## Slide 13: Trim Masks
Use another lithography step to get rid of undesired material
  Second mask
  Only use to get rid of unnecessary patterns
https://ieeexplore.ieee.org/document/7723830

## Slide 14: Trim Masks
Overlay becomes a problem
  Alignment of the second mask becomes a consideration
https://ieeexplore.ieee.org/document/7723830

## Slide 15: Trim Masks
Second SADP Lithography step is simpler than a second LELE Lithography step
  Cheaper
  Less Critical
https://semiengineering.com/self-aligned-double-patterning-part-one/

## Slide 16: Self Aligned Quadruple Patterning
“Double SADP”
Doubles resolution
Two trim lithography steps
Nakatama, K; et al. SPIE 2012

## Slide 17: Self Aligned Quadruple Patterning
Nakatama, K; et al. SPIE 2012

## Slide 18: SADP Problems
Not all patterns can be printed
Primary and secondary patterns can’t touch
https://http://www.aspdac.com/aspdac2013/archive/pdf/3C-4.pdf/

## Slide 19: SADP Problems
Anti-parallel line ends
  Trim masks overlap if they are too close
https://ieeexplore.ieee.org/document/7723830

## Slide 20: SADP Problems
Turns are difficult to control
  Unideal patterning results
https://ieeexplore.ieee.org/document/7723830

## Slide 21: SADP Problems-Via Manufacturing
Via manufacturing with SADP or single patterning is not possible
  Requires another double lithography technique
https://ieeexplore-ieee-org.ezproxy.lib.utexas.edu/document/7940014

## Slide 22: Via Manufacturing
Double manufacturing with half absorbance
The common exposed areas are fully exposed

## Slide 23: Via Manufacturing
After etching, unexposed areas form holes
Holes can be filled with a conductive via material

## Slide 24: Via Manufacturing
Via connects different layers of materials
Other layers formed from other types of patterning

## Slide 25: In Practice
Company | Logic Process | MMP Patterning Technique | Production Start
Intel | 14nm | SADP | 2014
Intel | 10nm | SAQP | end of 2018
TSMC | 16FF | LELE | 2015
TSMC | 10FF | SADP | 2017
TSMC | 7FF | SADP | early 2017
Samsung | 14LP* | LELE | 2015
Samsung | 10LPE | LELELE | end of 2016
Samsung | 8LPP | LELELELE | end of 2018
Global-Foundries | 7LP | SADP | 2018
Patterning Method | Normalized Wafer Cost
193i SE | 1
193i LELE | 2.5
193i LELELE | 3.5
193i SADP | 2
193i SAQP | 3
EUV SE | 4
EUV SADP | 6

## Slide 26: Conclusions
SADP along with other multiple patterning techniques will continue to be useful
  Combination of multiple patterning techniques
Design considerations will dominate what manufacturing method is used
Future innovations in multiple patterning are required to continue Moore’s Law until NGL’s are feasible

## Slide 27
Questions?

## Slide 28: References
Self-Aligned Double Patterning Lithography Aware Detailed Routing With Color Preassignment - IEEE Journals & Magazine, ieeexplore.ieee.org/document/7723830.
Self-Aligned Double Patterning-Aware Detailed Routing with Double via Insertion and via Manufacturability Consideration - IEEE Conference Publication, ieeexplore.ieee.org/document/7544285.
“Fill/Cut Self-Aligned Double-Patterning.” Semiconductor Engineering, semiengineering.com/fillcut-self-aligned-double-patterning/.
Mack, Chris. “Lecture 59 (CHE 323) Lithography Double Patterning.” YouTube, YouTube, 8 Nov. 2013, www.youtube.com/watch?v=Foush3X7dCc.
Nakayama, Koichi, et al. “Self-Aligned Double and Quadruple Patterning Layout Principle.” Search the World's Largest Collection of Optics and Photonics Applied Research., International Society for Optics and Photonics, 14 Mar. 2012, www.spiedigitallibrary.org/conference-proceedings-of-spie/8327/83270V/Self-aligned-double-and-quadruple-patterning-layout-principle/10.1117/12.916678.full.
“Self-Aligned Double Patterning, Part One.” Semiconductor Engineering, semiengineering.com/self-aligned-double-patterning-part-one/.
“Triple Patterning and Self-Aligned Double Patterning (SADP).” Tech Design Forum Techniques, www.techdesignforums.com/practice/guides/triple-patterning-self-aligned-double-patterning-sadp/.